## Slide 1
Characteristics of High-Power Diode-Laser Welds for Industrial Assembly
by
C.A. Walsh*, H.K.D.H. Bhadeshia*, A. Lau+, B. Matthias+, R. Oesterlein+, J. Drechsel°
* Department of Materials Science and Metallurgy, University of Cambridge, UK
+ ABB Corporate Research, Ladenburg, Germany
° Laserinstitut Mittelsachsen e.V., Mittweida, Germany
presented at the
20th International Congress on ICALEO 2001
Notes: Acknowledgement to conference organizers.
Brief description of authors and research cooperation between Cambridge University and ABB.

## Slide 2
Acknowledgement
Special thanks to the Laser Institute of Mittweida University
for the preparation of weld samples ...
Notes: Special acknowledgement to Mittweida University for providing access to laser welding set up for the generation of weld samples.

## Slide 3
Introduction
High Power Diode Laser becomes more promising in Welding Applications
Literature Survey
Advantages of High Power Diode Laser - HPDL
• High electrical-to-optical conversion efficiency
• Increasing output power density
• More compact than other laser systems e.g. CO2 & Nd:YAG
Notes: HPDL is gaining popularity as higher output power becomes available.
Research recently published indicates the growing interest in HPDL systems.

## Slide 4
Experimental Setup
Laser Optics
• 2.2 kW JOLD 1000 diode laser
• 1 mm beam , 50 mm focal length lens, direct focusing on workpiece
Low Carbon Steel Material Composition
Weld Configuration
• 2mm thick single sheet of D52X
• 1.0, 1.4 and 2.23 kW powers and welding times of 0.15-2.65 s
Spot Weld
• Lap joint configuration (40x110 mm sheets with 20 mm overlap)
Stitch Weld
• Ar shielding gas used in all cases
• 2 x 0.77mm thick sheets of DC04
• Welding speeds of 10-50 mm/s and stitch lengths 5-20 mm
• Laser power of 1.4 and 2.26 kW
• With/without Ar shielding gas
Notes: Note the higher carbon and manganese content of D52X.

## Slide 5
Weld Shape - Spot Weld
Power = 1.4 kW
Power = 2.5 kW
0.65 s
1.15 s
1.65 s
2.15 s
2.65 s
0.15 s
0.65 s
2.65 s
0.15 s
1.15 s
1.65 s
2.15 s
0.21 s
0.195 s
0.18 s
0.165 s
0.15 s
0.225 s
2 mm
Power = 1.0 kW
Notes: At low powers get conduction mode welding.
At intermediate powers and longer times start getting the formation of a keyhole.
At the highest powers a keyhole is clearly present in all the welds.
Good weld fusion zones with very few pores.

## Slide 6
Weld Shape - Stitch Weld at 2.26 kW Laser Output
Laser beam
Keyhole
Laser beam
Fusion Zone
Notes: Full penetration welds can be formed at speeds of 40 mm/s with a 2.26 kW laser beam and at 10 mm/s with a 1.4 kW beam.
The weld fusion zones are in generally pore free and without significant defects of any other sort.
Without the use of a shielding gas the welds are more parallel sided but the fusion zones are smaller.
Difference with and without the use of shielding gas will be explained later by the energy transfer model.

## Slide 7
Weld Shape - Stitch Weld at 1.4 kW Laser Output
With Ar shielding gas
2mm
v=15mm/s; L=10mm
v=12mm/s; L=20mm
v=12mm/s; L=10mm
v=18mm/s; L=20mm
v=18mm/s; L=10mm
v=15mm/s; L=20mm
v=10mm/s; L=20mm
Without shielding gas
Notes: More micrographs on the stitch welds produced at lower laser power.

## Slide 8
0.5 mm
Weld Shape - Stitch Weld Micrographs
2.23 kW, 0.18 s with shielding gas
2.26 kW, 40 mm/s with shielding gas
1.4 kW, 12 mm/s with no shielding gas

## Slide 9
Energy Transfer Model
Energy Transfer Efficiency:
Melting Efficiency:

=
Heat absorbed by workpiece
Laser beam power

m
=
Energy used to melt workpiece
Heat absorbed
=


A
h

qo
Seam weld:
=

V
h

qo
t
where
[Fuerschbach (1996)]
Spot weld:
Fuerschbach’s Model:

m, seam

m, spot


=

0.48 - 0.29exp
(

6.8
)
- 0.17exp

59
)]
(

=
2
A
2
and

=
qo
2
h
Notations:
 - thermal diffusivity at the liquidus temperature (5.5 mm2/s)
 - welding speed
qo - laser beam power
A - cross-sectional area of the weld
h - enthalpy of melting
(10.4 J/mm3 )
V - volume of the fusion zone
t - welding time
Notes: Fuershbach measured the energy transfer efficiency of CO2 laser welds in several different materials and produced a material-independent model for the efficiency in terms of two dimensionless parameters.
Note:
Fuershbach’s equation is independent of material.
The only unknown quantity is the transfer efficiency so we can use this equation and best fit from experimental data to estimate the transfer efficiency.

## Slide 10
0.00
0.05
0.10
0.15
0.20
0.25
0.30
0.35
0.40
0.50
1.0
1.5
2.0
2.5
spot welds with shielding gas
stitch welds with shielding gas
stitch welds without shielding gas

m
Laser Output Power (kJ)
0
20
40
60
80
100
120
0
50
100
150
200
250
300
350
400
1.4kJ; with shielding gas
1.4kJ; without shielding gas
2.26kJ; with shielding gas
2.26kJ; without shielding gas
Model with shielding gas
Model without shielding gas


Energy Transfer Efficiency Results
Fuerschbach’s Model

= 0.57

= 0.42
Notes: Calculated from the fusion zone dimensions of each weld
A higher proportion of energy is used to melt the metal at higher laser powers.
Fuerschbach showed that  for CO2 laser welds increases with laser power.
Energy transfer efficiency is significantly lower when no shielding gas is used.

## Slide 11
Hardness Measurements
Objective: to maintain material homogeneity between weld & original metal
100
200
300
400
500
0
500
1000
1500
2000
2500
3000
3500
4000
spot welds
stitch welds with shielding gas
stitch welds without shielding gas
Vicker's Hardness
Energy per unit distance (J/mm)
100
200
300
400
500
0
20
40
60
80
100
120
140
Vicker's Hardness

m
Energy per unit distance (J/mm)
spot welds
stitch welds with shielding gas
stitch welds without shielding gas
Applied energy per unit distance =
{
qo/ for stitch weld
qot/d for spot weld, where d = beam 
Energy used for melting per unit distance =
Definitions:
m
x applied energy per unit distance
Notes: Spot welds are significantly harder than stitch welds.
Stitch welds without shielding gas are less hard than those with shielding gas.

## Slide 12
Hardness Determinants
allotriomorphic
ferrite
Widmanstätten
bainite & ferrite
Notes: Cooling rate
Composition

## Slide 13
50m
SPOT WELD
STITCH WELD
38.3J/mm; 1 kJ 2.15 s; 325 HV
39.4 J/mm; 1.4 kJ
10 mm/s; 165 HV
Microstructures
Notes: Similar values of the energy used to melt the fusion zone (38.3 and 39.4 J/mm).
Spot weld: faster cooling rate, D52X has higher C and Mn content
fewer reconstructive transformations, more displacive transformations
allotriomorphic and Widmanstätten ferrite, bainite and martensite
Stitch welds: slightly slower cooling rate, DC04 contains lower C and Mn content
weld metal transformed at higher temperatures
allotriomorphic and Widmanstätten ferrite only

## Slide 14
Tensile Shear Strength
1
2
3
4
5
6
7
0
10
20
30
40
50
60
70
80
Maximum tensile load (kN)
Volume (mm
3
)
British Standard BS1140
E.g.
Sheet thickness - 0.8mm
Min. TS - 280 Nmm-2
Required nugget - 4.5mm  (5thickness)
Min. Tensile Load = 3.6kN
Resistance Spot Weld
Min. Tensile Load = 3.6kN
Notes: Given a typical min. weld strength value & nugget size for resistance spot lap welds, the corresponding stitch weld can be determined accordingly.
We used 0.77mm thick sheet in DC04 metal with tensile strength of 294 N/mm2.
Weld strength depends on volume
Welds with volume > 20mm3 have strength exceeding 3.6 kN

## Slide 15
1
2
3
4
5
6
7
0.0
0.5
1.0
1.5
2.0
2.5
Linear fit to all data
Full penetration welds
Incomplete penetration
Maximum tensile strength (kN)
Ratio
stitch length : Wang's length
Weld Strength Model - Wang’s Length
Notes: This is based on work done by Wang (reference 17), who:
correlated the fatigue strength of laser welds with the fatigue strength of resistance spot welds,
calculated a set of laser weld dimensions (length and width) which could be used to replace resistance spot welds of diameter and yet have the same fatigue strength.
We want to
compare the strength of our welds with joints in currently used in industry
be able to calculate the required weld dimensions to produce a weld of a specified strength
Procedure:
Measured the length and the width of each weld at the faying surfaces
Used the measured weld width and Wang's table of weld dimensions to find his recommended length (Wang length)
Plot the ratio of the actual length to the Wang length against the measured tensile strength.
Note:
large data points are for full penetration welds
linear relationship between the maximum tensile strength and ratio of actual length to Wang length
all welds of dimensions equal to or exceeding those recommended by Wang (ratio >1) have a strength of 3.9kN or more
Conclusion:
Wang's data can be used as guidelines for suitable weld dimensions and the modelling of tensile strength measurements.

## Slide 16
Conclusions
1. Stitch welds in the lap configuration as produced using the HPDL system had the following characteristics:
  defect free
  full penetration
  low increase in hardness of the fusion zone (40-80 HV)
  strength depends on weld fusion zone volume & is comparable to that of other laser welds
2. Microstructure & hardness is sensitive to cooling rate and metal composition.
3. Models from the CO2 laser seam welding process have been successfully applied to HPDL stitch welding.
4. Energy transfer efficiency of the stitch welding process was calculated using known models, giving values of 0.57 and 0.42 for welding with and without the use of an Ar shielding gas.
5. Stitch welds produced using the high power diode laser system are comparable to resistance spot welds in terms of strength performance.
Notes: 2. This latter, in particular, must be taken into account when determining suitable weld operating parameters. An empirical confirmation on the cooling behaviour is much to be desired. - these comments you could make verbally?