## Slide 1
Thermodynamic functions
Equilibrium state
Case study: mechanical alloying
Computer calculation: phase diagrams
Thermodynamics - irreversible
Quasichemical models
Thermodynamics
H. K. D. H. Bhadeshia
https://www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 2
difference in molar volume
MgO-NiO 2.5%
MgO-MnO 17.5%
Kerrick, Darken. Geochimica et Cosmochimica Acta. 39(1975) 1431.

## Slide 3
Praseodymium-neodymium solid solutions
Lundin, Pool: J. Less Common Metals 9 (1965) 48-53

## Slide 4
Evolution of solutions
solution
compound

## Slide 5
mechanical alloying
cast-iron
balls
powder

## Slide 6
extrusion of canned powder
image courtesy of Jan-Olof Nilsson
Sandvik Materials Technology.
Extrusion of stainless steel.

## Slide 7
200 nm
“MA956” Fe-20Cr-4.5Al-0.5Ti-0.5 yttria wt%
large driving force for recrystallisation

## Slide 8
“MA6000”
Ni-15Cr-4.5Al-2.3Ti-4W-1.1 yttria wt%
200 nm
large driving force for recrystallisation

## Slide 10
Helical grains

## Slide 12
not recrystallised

## Slide 13
Micrograph courtesy of
R. Errichello, GEARTECH

## Slide 14
How do we know that mechanical processing results in a true solution?

## Slide 15
MA956

## Slide 16
Chou & Bhadeshia

## Slide 18
Probability of pairwise bonds in random solution

## Slide 19
o
o
A
B
A
B
1-x
Gibbs free energy per mole
Concentration x of B
m
m
free energy of
mechanical
mixture
G*
x
Mechanical Mixture

## Slide 20
o
o
A
B
A
B
x
Gibbs free energy per mole
Composition
m
m
G{x}
free energy of
mechanical
mixture
∆G
M
free energy
of solution
G*

## Slide 21
+
=
configurational entropy?

## Slide 22
For a random mixture, number of configurations given by:

## Slide 24
Solution-like behaviour when particles about 1000 atoms in size
Free energy of mixing due to configurational entropy alone

## Slide 25
Enthalpy
chemical component of interfacial energy

## Slide 26
Structural component of
interfacial energy
Sv
Particle size
Solution formation impossible!

## Slide 27
coherent
coherent
incoherent

## Slide 28
Single barrier to solution formation when components attract

## Slide 29
Double barrier to solution formation when components immiscible

## Slide 31
o
o
A
B
A
B
Gibbs free energy per mole
m
m
Concentration x of B
Paradox at concentration extremities vanishes in the discrete model of concentration

## Slide 32
Austenite exists simultaneously in two magnetic states
High-volume, high magnetic moment, ferromagnetic
Low-volume, low magnetic moment, antiferromagnetic
Therefore, its overall expansion coefficient is much greater than that of ferrite

## Slide 33
Experimental proof: force large lattice parameter by alloying with copper – unfortunately, Fe & Cu do not dissolve into each other.
Prepare Fe-Cu solution by mechanical alloying.
At low Fe concentrations, magnetic moment per iron atom is 2.3 µb, ambient conditions.
At large Fe concentrations, less than 1 µb.