Table-1   Chemical compositions of the workpiece material [38]

| C | Si | Mn | Cr | Mo | Ni | V | N |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.07 | 0.10 | 0.92 | 0.04 | < 0.01 | 0.03 | < 0.01 | 0.005 |

Table-2	Incident laser powers and on-times used in the experiments

and the corresponding cooling rate parameters, C1 and C2, as

determined from the numerical analyses.

|  | Laser Power in Watt |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1000 |  | 1400 |  |  | 2230 |  |  |
| On-time (s) | C1 | C2 | On-time (s) | C1 | C2 | On-time (s) | C1 | C2 |
| 0.15 | 94.816 | 166.17 | 0.15 | 105.98 | 179.16 | 0.15 | 18.007 | 145.15 |
| 0.65 | 19.848 | 159.99 | 0.65 | 20.218 | 184.52 | 0.165 | 16.016 | 144.27 |
| 1.15 | 23.789 | 232.77 | 1.15 | 27.923 | 277.99 | 0.180 | 14.224 | 147.22 |
| 1.65 | 30.887 | 306.58 | 1.65 | 41.344 | 388.11 | 0.195 | 10.802 | 141.78 |
| 2.15 | 43.286 | 407.81 | 2.15 | 56.702 | 520.94 | 0.210 | 9.4920 | 144.98 |
| 2.65 | 57.435 | 529.91 | 2.65 | 61.998 | 583.07 | 0.225 | 8.0715 | 145.03 |

Table 3	Predicted volume fractions (%) of the austenite decomposition products

in the fusion zone of the spot welds. The prior austenite grain size and the

cooling time, t8/5, of the cooling curve used in the calculations are also given.

| Power (kW) | On-time (s) | t8/5 (s) | Grain Size (m) | Model 1 |  |  | Model 2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | f (%) | w (%) | Martensite (%) | f (%) | w (%) | Martensite (%) |
| 1.0 | 0.15 | 0.07 | 22 | 0 | 0 | 99 | 0 | 0 | 100 |
| 1.0 | 0.65 | 0.30 | 37 | 0 | 0 | 99 | 1 | 0 | 99 |
| 1.0 | 1.15 | 0.83 | 41 | 0 | 0 | 99 | 22 | 1 | 77 |
| 1.0 | 1.65 | 1.21 | 46 | 20 | 61 | 19 | 24 | 4 | 72 |
| 1.0 | 2.15 | 1.44 | 47 | 31 | 55 | 14 | 25 | 6 | 68 |
| 1.0 | 2.65 | 1.55 | 62 | 27 | 43 | 30 | 21 | 7 | 72 |
| 1.4 | 0.15 | 0.08 | 20 | 0 | 0 | 99 | 0 | 0 | 100 |
| 1.4 | 0.65 | 0.49 | 31 | 0 | 0 | 99 | 15 | 0 | 85 |
| 1.4 | 1.15 | 1.09 | 37 | 0 | 0 | 99 | 27 | 3 | 70 |
| 1.4 | 1.65 | 1.39 | 44 | 31 | 59 | 9 | 27 | 6 | 67 |
| 1.4 | 2.15 | 1.54 | 53 | 30 | 49 | 20 | 24 | 8 | 69 |
| 1.4 | 2.65 | 1.60 | 54 | 31 | 48 | 21 | 23 | 8 | 68 |
| 2.23 | 0.15 | 0.22 | 22 | 0 | 0 | 99 | 0 | 0 | 99 |
| 2.23 | 0.165 | 0.25 | 24 | 0 | 0 | 99 | 0 | 0 | 99 |
| 2.23 | 0.180 | 0.30 | 22 | 0 | 0 | 99 | 1 | 0 | 98 |
| 2.23 | 0.195 | 0.34 | 24 | 0 | 0 | 99 | 2 | 0 | 97 |
| 2.23 | 0.210 | 0.42 | 27 | 0 | 0 | 99 | 8 | 0 | 91 |
| 2.23 | 0.225 | 0.50 | 26 | 0 | 0 | 99 | 16 | 1 | 83 |

Fig.1    Temperature dependent thermal conductivity and specific heat of the material

Fig. 2	Transverse section considered for the present analysis

Fig.3	Schematic presentation of the ‘Double-ellipsoidal’ distribution of the laser

beam.

Fig.4	Comparison of calculated and measured weld pool width as measured on the

upper surface

Fig.5	Comparison of calculated and measured weld penetration

Fig.6	Variation of cooling rate with weld pool temperature for 1.0 kW laser power

Fig.7	Variation of cooling rate with weld pool temperature for 1.4 kW laser power

Fig.8	Variation of cooling rate with weld pool temperature for 2.23 kW laser power

Fig.9	Ratio of the values for heat flow parameters, C1 and C2, obtained using finite element

analysis with those obtained from a simple analytical model