## Slide 1
Introduction and point groups
Stereographic projections
Low symmetry systems
Space groups
Deformation and texture
Interfaces, orientation relationships
Martensitic transformations
Crystallography
H. K. D. H. Bhadeshia
https://www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 2
www.phase-trans.msm.cam.ac.uk/2020/Crystallography_book.pdf
(hard copies of both in departmental library)

## Slide 3
crystalline
amorphous
cristobalite from
glassy magma

## Slide 4
anisotropic molecules
solid crystal, ordered
liquid crystal,
somewhat ordered
liquid: cannot support
shear stress

## Slide 5
Form

## Slide 6: Anisotropy (elastic modulus, MPa)
Ag
Mo

## Slide 7: Polycrystals

## Slide 8: 2D lattices

## Slide 13
The Lattice

## Slide 14: Graphene, nanotubes

## Slide 29
P
I
F

## Slide 31
height 1/2
height 0,1
hcp Fe
6
3

## Slide 32: Centre of symmetry and inversion

## Slide 33
180°120°90°60°

## Slide 35: Bravais Lattices
Triclinic P
Monoclinic P & C
Orthorhombic P, C, I & F
Tetragonal P & I
Hexagonal
Trigonal P
Cubic P, F & I

## Slide 36
Bravais Lattices

## Slide 37
Bundy (1965)
pure iron

## Slide 39
Paxton et al. (1990)
Pure iron

## Slide 40
Fe
Ru
Os
Hs
6d 2s

## Slide 41
Introduction and point groups
Stereographic projections
Low symmetry systems
Space groups
Deformation and texture
Interfaces, orientation relationships
Martensitic transformations
Crystallography
H. K. D. H. Bhadeshia
www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 42
1/2
1/2
1/2
1/2
Crystal Structure

## Slide 44
lattice + motif = structure
primitive cubic lattice
motif = Cu at 0,0,0
Zn at 1/2, 1/2, 1/2

## Slide 45
1/4
1/4
1/4
1/4
1/4
3/4
3/4
3/4
3/4
Lattice: face-centred cubic
Motif: C at 0,0,0 C at 1/4,1/4,1/4

## Slide 47
1/4
1/4
3/4
3/4

## Slide 48
x

## Slide 49
1/4
1/4
3/4
3/4
Lattice: face-centred cubic
Motif: Zn at 0,0,0 S at 1/4,1/4,1/4

## Slide 52
fluorite

## Slide 55: Rotation axes
2 diad
3 triad
4 tetrad
6 hexad

## Slide 57
CENTRE OF SYMMETRY

## Slide 58: Point groups
2m

## Slide 60: Sulphur tetraflouride
Water and sulphur tetrafluoride have same point symmetry and hence some identical vibration modes - similar lines in spectra

## Slide 61: Gypsum
2/m

## Slide 62: Epsomite
222

## Slide 64
3m
bishop

## Slide 65
castle
4/mmm

## Slide 66
1 µm
hexagonal
aluminium
nitride
Courtesy Shaumik Lenka

## Slide 69: without high-order axes

## Slide 70: with high-order axes

## Slide 72: Weiss Law
If a direction [uvw] lies in a plane (hkl) then
uh+vk+wl = 0
[uvw]
(hkl)

## Slide 73
[110]
(110)
x
y
z
y
x
z