## Slide 1
Introduction and point groups
Stereographic projections
Low symmetry systems
Space groups
Deformation and texture
Interfaces, orientation relationships
Martensitic transformations
Crystallography
H. K. D. H. Bhadeshia

## Slide 3
Ga0.52In0.48P
lattice point
When epitaxially deposited,
undergoes ordering of atoms that leads to a change from a cubic-F (point group 43m) to a trigonal structure (point group 3m)
_

## Slide 4
3m
trigonal
polar group
mirror plane

## Slide 5
6mm
hexagonal
polar group
mirror plane

## Slide 6
polar group 6mm GaN

## Slide 7
Experimental data
Chemical formula: TiPbO3
X-rays: tetragonal lattice
X-rays: cell volume
Density: 1Pb, 1Ti, 3O therefore P-lattice
Valency: Ti4+, Pb2+, O2-
Piezoelectric
Where are the atoms in the cell?

## Slide 8
to locate 3 O ions they would have to be at the face-centres
the titanium and lead would be at equivalent point symmetries
titanium with its greater valency would have a larger number of oxygen ions
in its vicinity than lead

## Slide 9
tetragonal

## Slide 10
Point group 4mm, tetragonal
a general location x,y,z with a site symmetry 1
would require 8 such atoms in the cell

## Slide 11
P4mm

## Slide 12
site symmetry
2mm
4mm
4mm
4mm

## Slide 14
1 oxygen
2 oxygens
face centres
face centre
1 lead
corner
✘
✘

## Slide 15
the titanate just discussed has no centre of symmetry,
piezoelectric.
free energy of heterogeneous solution

## Slide 16
yellow atoms
are sulphur
Carles Millan, Wikimedia, CC BY-SA 3.0

## Slide 17
Pyrite m3

## Slide 19
Stereograms for systems of low symmetry

## Slide 20
5
2,3,8

## Slide 21
2,3,8 2,3,5

## Slide 22
2,3,5
normals directions

## Slide 23
plotting poles, i.e.,
plane normals

## Slide 27
Weiss zone rule