## Slide 1
Introduction and point groups
Stereographic projections
Low symmetry systems
Space groups
Reciprocal Lattice & Diffraction
Deformation and texture
Interfaces, orientation relationships
Martensitic transformations
Crystallography
H. K. D. H. Bhadeshia

## Slide 2
vector has magnitude and direction
u
u

## Slide 9
the basis vectors of the reciprocal lattice are not necessarily parallel
to those of the real-space lattice

## Slide 12
Construct reciprocal
lattice section normal
to [001]

## Slide 13
Cubic P, section of reciprocal lattice normal to [001]

## Slide 14
Reciprocal lattice
section normal
to [110]

## Slide 15
Cubic P, section of reciprocal lattice normal to [110]

## Slide 17
Cubic P, section of reciprocal lattice normal to [111]

## Slide 21
For 100 keV accelerating voltage, the wavelength of electrons is 0.0037 nm.
If the d spacing is 0.2 nm, then the Bragg angle is just 0.5°

## Slide 22
Consider now the Bragg law in reciprocal space

## Slide 24
Cubic P
Cubic F

## Slide 25
Cubic P [011]
Cubic F
_
111

## Slide 26
Cubic P [111]
Cubic F
022
_
220
_

## Slide 28
Diffraction from thin crystals

## Slide 31
200 nm thick foil
50 nm thick foil

## Slide 32
[111]
[1 1 0.9]

## Slide 33
(R. Herring)

## Slide 37
Cubic-F
lattice parameter 3.566 Å

## Slide 38
electron diffraction

## Slide 40
Su et al.
2014