## Slide 1
Introduction and point groups
Stereographic projections
Low symmetry systems
Space groups
Reciprocal Lattice & Diffraction
Deformation and texture
Interfaces, orientation relationships
Martensitic transformations
Crystallography
H. K. D. H. Bhadeshia
Notes: Today I am going to talk about a phase transformation that can occur in the solid-state, in the absence of diffusion.

## Slide 2
can form at incredibly
low temperatures
can form very rapidly
no composition change
Diffusionless

## Slide 3
shape

## Slide 4
Acta Metallurgica 13 (1965) 99-107

## Slide 5
Irrational: why?

## Slide 6
NISHIYAMA-WASSERMAN

## Slide 7
KURDJUMOV-SACHS

## Slide 8
actual orientation
irrational

## Slide 11
Glissile interface cannot contain more than one set of dislocations.
Martensitic transformation only possible if deformation which changes the parent into the product leaves one line undistorted and unrotated, i.e. an invariant-line.
Deformation is an invariant-line strain.

## Slide 16
movie courtesy of
Professor Toshihiko Koseki

## Slide 17
d
s
1
s
1
d
1
uniaxial dilatation
simple shear
general invariant-plane strain
s=0.26
d=0.03

## Slide 18
c
r
d
s
1
Christian, 1957

## Slide 21
The Bain strain

## Slide 22
[100]
[001]
o
a
a'
b
b'
o
b'
b
a,a'
(a)
(b)

## Slide 24
Austenite
(a)
w
x
y
z
Twinned
Martensite
Twin
Boundary
Correct macroscopic shape, correct structure
x
w
z
y
z
Slipped
Martensite
LATTICE
-INVARIANT
DEFORMATION
x
w
y
Observed
shape,
wrong
structure
P
(b)
w
x
z
y
1
RB
(c)
x
w
z
y
P
2
Martensite
(wrong
shape)

## Slide 26
image courtesy of Professor Tadashi Maki
transformation
twins