## Slide 1
Martensite
Bainite
Alloy design: strong bainite
Widmanstaetten ferrite
Allotriomorphic ferrite
Pearlite
Overall kinetics
TRIP steel
TWIP steel
Mitigation of residual stress
Bulk nanostructured steel
Steels
H. K. D. H. Bhadeshia
www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 3
hard
quenched
plates or laths
displacive
volume change
brittle
body-centred tetragonal
metastable
diffusionless

## Slide 4
Materials, transformation temperatures & strength

## Slide 5
Olson and Hartman, 1982

## Slide 6
Olson and Hartman, 1982

## Slide 7
Olson and Hartman, 1982

## Slide 8
Courtesy of Professor Koichi Tsuchiya, Toyohashi University of Technology

## Slide 9
can form at incredibly
low temperatures
can form very rapidly
no composition change
Diffusionless

## Slide 10
shape

## Slide 12
Irrational: why?

## Slide 13
Shape of martensite ?

## Slide 14
NISHIYAMA-WASSERMAN

## Slide 15
KURDJUMOV-SACHS

## Slide 16
actual orientation
irrational

## Slide 17
athermal transformation

## Slide 18
Fe-0.05C-24Ni-3Mn-0.2Cu wt%
Kurdjumov & Maximova

## Slide 22
Glissile interface

## Slide 26
Glissile interface cannot contain more than one set of dislocations.
Martensitic transformation only possible if deformation which changes the parent into the product leaves one line undistorted and unrotated, i.e. an invariant-line.
Deformation is an invariant-line strain.

## Slide 31
Wirtschaftsvereinigung Stahl, Düsseldorf
courtesy of Professor Hans Werner Zoch

## Slide 32
M. Benke, V. Mertinger, Institute of Physical Metallurgy, Metalforming and Nanotechnology, University of Miskolc
http://www.matsci.uni-miskolc.hu/new/

## Slide 33
d
s
1
s
1
d
1
uniaxial dilatation
simple shear
general invariant-plane strain
s=0.26
d=0.03

## Slide 34
c
r
d
s
1
Christian, 1957