## Slide 1
Martensite
Bainite
Alloy design: strong bainite
Widmanstaetten ferrite
Allotriomorphic ferrite
Pearlite
Overall kinetics
TRIP steel
TWIP steel
Mitigation of residual stress
Bulk nanostructured steel
Steels
H. K. D. H. Bhadeshia
www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 2
Tailored blanks

## Slide 3
Inner panels of both doors and side panel use tailored blanks

## Slide 4
aluminium-killed
TRIP-steel
Mizui et al. (1997)

## Slide 5
Fe-30.5Ni-0.32C wt%,
Ms = -80°C
Stefan Forsik
shape deformation

## Slide 6
orthonormal coordinates

## Slide 7
u
v

## Slide 10
Bhadeshia, 1982

## Slide 11
s
50 mm
polycrystalline austenite
Bhadeshia, 1982

## Slide 14
tensile axis
= 15%
41.7°

## Slide 15
Austenitic stainless steel
(Courtesy Prof. N. Tsuji)
25 ∘C
200 ∘C

## Slide 16
Gao et al. (2019)

## Slide 17
TRIP steels that are fully austenitic are expensive
How do we produce cheap austenite?

## Slide 18: TRIP-Assisted Steels
too much carbon is bad
Jae Hoon Jang, In Gee Kim
austenite is expensive
carbon can be cheap
Notes: 18

## Slide 20
Typical composition Fe-0.15C-1.5Si-1.5Mn wt%

## Slide 21
Typical microstructure:
70% allotriomorphic ferrite
16% bainitic ferrite
14% retained austenite
2.1% elongation due to TRIP

## Slide 22
aluminium-killed
TRIP-steel
Mizui et al. (1997)
work hardening!

## Slide 23
Elongation of TRIP-assisted steel
not due to transformation plasticity
work hardening due to hard martensite

## Slide 26
Corten is a weathering steel with 0.25-0.55Cu and 0.5-1.25Cr wt% develops a patina

## Slide 27: TRIP-Assisted Steels
too much silicon is bad
Notes: 27

## Slide 35
Notes: 35

## Slide 36
tested at room temperature
14.3% 
7% 

## Slide 37
tested at 100 °C
14.3% 
13% 

## Slide 38
Notes: 38

## Slide 39
(Prof. Hongliang Yi, Northeastern University, China)
continuous casting
after hot-rolling

## Slide 40
(Prof. Hongliang Yi, Northeastern University, China)
after cold-rolling

## Slide 41
(Prof. Hongliang Yi, Northeastern University, China)
after continuous annealing