## Slide 1
Martensite
Bainite
Alloy design: strong bainite
Widmanstaetten ferrite
Allotriomorphic ferrite
Pearlite
Overall kinetics
TRIP steel
TWIP steel
Mitigation of residual stress
Bulk nanostructured steel
Steels
H. K. D. H. Bhadeshia
www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 2
mechanical twinning

## Slide 4
A
B
CA
B
A
B CBC
A
B CBA

## Slide 6
Frommeyer, Brux and Neumann

## Slide 7
Frommeyer, Brux and Neumann
dynamic Hall-Petch effect

## Slide 8
TWIP Steels
Fe-25Mn-3Si-3Al wt%
density 7.3 g cm-3
fully austenitic
maintain attractive properties to -150°C
and at high strain rates (103 s-1)
data from Frommeyer et al.

## Slide 9
delayed fracture
difficult to produce
high thermal expansion
Bruno de Cooman

## Slide 10: Atomic traps for hydrogen
Fe
Al
Song, Bhadeshia, Suh, 2014

## Slide 11
Sanjeev Sharma and Richard Dashwood of the International Manufacturing Centre, WMG University of Warwick.

## Slide 12
courtesy of
Professor Wolfgang Bleck

## Slide 14
https://www.stahl-innovationspreis.de/news/gewinner-2018-sichere-zuege-dank-stahlforschung-und-entwicklung/
Steel innovation award 2018
photo & graphics: DLR

## Slide 15
TRIP, TWIP:
transformation or twinning deformations under an external stress
enhanced work hardening
greater strength and ductility
Suppose a material develops internal stress:
can TRIP be used to stop that stress from developing?

## Slide 16
Weld: liquid metal solidifies, cools, contracts, stress
liquid
solid
contraction
Compensate for thermal contraction
Notes: 16

## Slide 17
Residual stress
Notes: 17

## Slide 18
Notes: 18

## Slide 19
Notes: 19

## Slide 20
Notes: 20

## Slide 21
Jones & Alberry, 1977
Notes: 21

## Slide 22
Charpy
fatigue
corrosion
tensile
critical stress intensity
Notes: 22

## Slide 23
Notes: 23

## Slide 24
Notes: 24

## Slide 25
Notes: 25

## Slide 26
Notes: 26

## Slide 27
Notes: 27

## Slide 28
Criteria for design of stainless steel consumable
Cr concentration > 12 wt%
Carbon concentration minimal
Low MS temperature but not too low
Suppress MS with solutes other than carbon
Capable of becoming fully austenitic
Solidification as -ferrite

## Slide 30
Dramatically reduced distortion
Leif Karlsson
Notes: 30