## Slide 1
Martensite
Bainite
Alloy design: strong bainite
Widmanstaetten ferrite
Allotriomorphic ferrite
Pearlite
Overall kinetics
TRIP steel
TWIP steel
Mitigation of residual stress
Bulk nanostructured steel
Steels: lecture 2 of 12
H. K. D. H. Bhadeshia
www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 4
The Bain strain

## Slide 7
Austenite
(a)
w
x
y
z
Twinned
Martensite
Twin
Boundary
Correct macroscopic shape, correct structure
x
w
z
y
z
Slipped
Martensite
LATTICE
-INVARIANT
DEFORMATION
x
w
y
Observed
shape,
wrong
structure
P
(b)
w
x
z
y
1
RB
(c)
x
w
z
y
P
2
Martensite
(wrong
shape)

## Slide 9
Transformation twins (Shibata, Maki)

## Slide 12
Tomota et al. 1988

## Slide 13
Austenite
(a)
w
x
y
z
Observed
shape,
correct
structure
P
(b)
w
x
z
y
1

## Slide 14
Brooks, Loretto and Smallman, 1979

## Slide 16
a
g
Carbon Concentration
Free Energy
x
x
x
ag
ga
Equilibrium transformation
a
g
Carbon Concentration
Free Energy
x
x
x
ag
ga
Composition invariant
transformation
T1

## Slide 18
T1

## Slide 20
What have we learnt so far that may be useful in design?

## Slide 21
Can calculate the complete crystallography.
Therefore, the transformation texture.
Kundu

## Slide 22
Therefore, boundaries become susceptible to impurity embrittlement.
Martensitic transformation – disciplined motion of atoms.
Plates cannot cross boudaries.

## Slide 23
Therefore, strong martensitic steels must be pure (low P, Sn … ) or contain solutes that getter impurities, e.g. Mo

## Slide 24
Can calculate the size and shape of martensite.
Therefore, can estimate mechanical behaviour.
General rule: make the structure fine for better properties.
How?

## Slide 25
Mathew Peet

## Slide 26
Kundu

## Slide 28
Fe-0.34C-1.5Si ….. wt%
untempered martensite