## Slide 1
Martensite
Bainite: mechanism based design
Alloy design: strong bainite
Widmanstaetten ferrite
Allotriomorphic ferrite
Pearlite
Overall kinetics
TRIP steel
TWIP steel
Mitigation of residual stress
Bulk nanostructured steel
Steels: bainite, lecture 4 of 12
H. K. D. H. Bhadeshia
www.phase-trans.msm.cam.ac.uk/teaching.html

## Slide 8
Jang, Kim, Bhadeshia (2009)
Notes: 8

## Slide 9
Simple, carbide-free alloys
Fe-0.4C-3Mn-2Si wt%
suppress
cementite
hardenability

## Slide 10
10

## Slide 11
Fine structure
Retained austenite:
TRIP effect
no ductile-brittle transition
barrier to hydrogen
No cementite
Small concentration of C in ferrite

## Slide 12
Very poor toughness!

## Slide 13
50 µm

## Slide 15
Carbide-free alloys
Fe-0.4C-3Mn-2Si
Fe-0.2C-3Mn-2Si
Fe-0.4C-4Ni-2Si wt%
Notes: 15

## Slide 17
0.5 μm

## Slide 21
Bain: alloying elements in steels (1939)

## Slide 23
image courtesy of pngimg.com
Creative Commons 4.0 BY-NC
https://creativecommons.org/licenses/by-nc/4.0/
wish to design
rail steels using
the carbide-free
bainitic steel

## Slide 24
Rail steel – requirements:
Rolling-contact fatigue.
Wear resistance.

## Slide 27
Yates, Jerath, Bhadeshia
Notes: 27

## Slide 28
carbide-free bainitic rail
Carbide-free bainite has no hard particles,
Just bainitic ferrite and retained austenite
Kevin Sawley: 90 million gross tonnes of traffic on curve

## Slide 29
Notes: 29

## Slide 30
November 2019: 1 billion gross tonnes of traffic achieved
Notes: 30

## Slide 31
Carbide-free bainitic rail in the tunnel has
completed >1000,000,000 gross tonnes of traffic
without developing fatigue, without need for grinding.
Pascal Secordel (Francerail), Jay Jaiswal (Arrail)
April 2020

## Slide 33: Advances in carbide-free bainitic steels
2500
2000
1500
1000
20
40
60
80
100
120
140
160
180
Ultimate tensile strength / MPa
Fracture toughness / MPa √m
18 wt% Ni
maraging steel
QT

## Slide 34
airbags, wheelchairs, tool holders
Ascometal

## Slide 35
Charpy 120 J at 25°C
Strength > 1100 MPa