## Slide 1
eT13= eT31 ≠0
all other components are zero
Elastic strain energy
Interaction energy
Ref. 133 Elastic strain energy and interactions

## Slide 3
Ref. 132 Thermoelastic martensite
 Calculation of plastic accommodation area by the transformation
of ellipsoidal plate
Obtain constrained shear stress σc13
Use Von mises criterion for yielding
σceff ≥ σy

## Slide 4
For single plate

## Slide 5
An assembly of plates with opposite shape strain
In an assembly, plastic zone diminishes
minimize the strains accommodation the transformation shape change
Total strain energy of the system is reduced.

## Slide 6
Free surface
Constrained strain = 0
At the tip, the same direction of strain favored
At the broad interface, opposite strain favored
Most of plastic zone exists on the broad interface.
Therefore, the minimization of strain energy can be realized when the broad interface are exposed to constrained strain minimized situation, in other word, free surface.
Interpretation