## Slide 1
For plotting : Graphic- plot options

## Slide 2
To plot in separate window – then edit –copy – paste in ImageJ-convert to png

## Slide 3
Before quant analysis – rest plot options

## Slide 4
Input for diffractometer geometry : The values change here makes little change in the Lorentz polarization factor

## Slide 6
Selection of incident radiation
1. Keep “detector- scintillation” and “instrument broadening = Cagliotti PV”

## Slide 7
Background function : Increase add parameter to 5 if 2theta > 120 degree

## Slide 8
Load A+ F+ M – 1 .cif( drag and drop) file in “phases” and check all parameters

## Slide 9
Calculate

## Slide 10
After computaion- check the matchof the profiles

## Slide 11
To shift the pear to the “left”, increase a/b/c.
To shift the pear to the “right”, decrease a/b/c.

## Slide 12
Change in high order polinomials of background makes abrupt changes , so restrict to pol 0 and pol1.

## Slide 13
Quantitative analysis