## Slide 1: Fundamentals of Rietveld Refinement I. XRD Pattern Simulation
An Introduction to Rietveld Refinement
using
PANalytical X’Pert HighScore Plus v3.0d
Scott A Speakman, Ph.D.
MIT Center for Materials Science and Engineering
speakman@mit.edu

## Slide 2: Outline
Calculating a Diffraction Pattern from a Crystal Structure
Using HighScore Plus to Simulate a Diffraction Pattern
Manually Refining a Model to Match Experimental Data

## Slide 3: The position and intensity of peaks in a diffraction pattern are determined by the crystal structure
These three phases of SiO2 are chemically identical.
Differences in the atomic structure are reflected in the diffraction patterns.
Notes: Quartz and cristobalite have two different crystal structures
  The Si and O atoms are arranged differently, but both have structures with long-range atomic order
  The difference in their crystal structure is reflected in their different diffraction patterns
The amorphous glass does not have long-range atomic order and therefore produces only broad scattering peaks

## Slide 4: The diffraction peak position is a product of the atomic bond distances in the crystal
Bragg’s Law: λ = 2dhklsinθ
Bragg’s law calculates the angle where constructive interference from X-rays scattered by parallel planes of atoms will produce a diffraction peak.
  In most diffractometers, the X-ray wavelength l is fixed.
  Consequently, a family of planes produces a diffraction peak only at a specific angle 2q.
  The lattice parameters of the unit cell are used to calculate dhkl

## Slide 5: dhkl is a function of the size and shape of the unit cell
dhkl is the vector drawn from the origin of the unit cell to intersect the crystallographic plane (hkl) at a 90° angle.
  dhkl, the vector magnitude, is the distance between parallel planes of atoms in the family (hkl)
  the diffraction peak position is a product of the average atomic distances in the crystal
  anything that changes the average bond distances (temperature, pressure, etc.) will change dhkl and therefore the diffraction peak positions
d110

## Slide 6: The amplitude of light scattered by a crystal is determined by the arrangement of atoms in the diffracting planes
The structure factor quantifies the amplitude of light scattered by a crystal
  The patterns of atoms in the unit cell scatters strongly in some directions and weakly in others owing to interference of the wavelets scattered by the atoms
Fhkl sums the result of scattering from all of the atoms in the unit cell to form a diffraction peak from the (hkl) planes of atoms
The amplitude of scattered light is determined by:
  where the atoms are on the atomic planes
    this is expressed by the fractional coordinates xj yj zj
  what atoms are on the atomic planes
    the scattering factor fj quantifies the relative efficiency of scattering at any angle by the group of electrons in each atom
    Nj is the fraction of every equivalent position that is occupied by atom j

## Slide 7: The scattering factor, f, quantifies the efficiency of scattering from a group of electrons in an atom
X-rays are electromagnetic radiation that interact with an electron, which reradiates the X-ray as a spherical wave
The number of electrons around an atom defines how strongly it will scatter the incident X-ray beam
  the initial strength of the atomic scattering factor is equal to the number of electrons around the atom
The scattering factor, f, is a product of several terms describing the interaction of the X-ray with the electrons around an atom

## Slide 8: The atomic scattering factor f0 can be found using tables or equations determined experimentally or from quantum mechanical approximations
f0 at 0° is equal to the number of electrons around the atom
  Y and Zr are similar, but slightly different, at 0°
  Zr and Zr4+ are slightly different at 0°
  Y3+ and Zr4+ are identical at 0°
the variation with (sin θ)/λ depends on size of atom
  smaller atoms drop off quicker
  at higher angles, the difference between Y3+ and Zr4+ is more readily discerned
  at higher angles, the difference between different oxidation states (eg Zr and Zr4+) is less prominent

## Slide 9: Thermal motion of the atom changes the scattering factor
the efficiency of scattering by an atom is reduced because the atom and its electrons are not stationary
  the atom is vibrating about its equilibrium lattice site
  the amount of vibration is quantified by the Debye-Waller temperature factor: B=8π2U2
    U2 is the mean-square amplitude of the vibration
  this is for isotropic vibration: sometimes B is broken down into six Bij anistropic terms if the amplitude of vibration is not the same in all directions.
  aka temperature factor, displacement factor, thermal displacement parameter

## Slide 10: Anomalous scattering of X-rays with energies near the absorption edge of the atom changes the scattering factor
scattering factor has a real and imaginary term
these terms only matter when the energy of the incident X-ray approaches the ionization energy of atom
  when the wavelength of the incident X-ray is near the absorption edge of the atom
anomalous scattering describes how some photons with energy approaching the ionization energy will be scattered out of phase with the majority of photons

## Slide 11: With a crystal structure to solve Bragg’s Law and Fhkl, you can calculate the diffraction pattern from an ideal crystal
Ideal powder diffraction patterns can be simulated if you know ...
  space group symmetry
  unit cell dimensions
  atom types
  relative coordinates of atoms in unit cell
  atomic site occupancies
  atomic thermal displacement parameters
... for each and every phase in the sample

## Slide 12: Where to Get Crystal Structures
publications
Commercial Databases
  Inorganic Crystal Structure Database (ICSD)
  Linus Pauling File (LPF)
    this is included in ICDD PDF4+ Inorganic
  NIST Structural Database (metals, alloys, intermetallics)
  Cambridge Structure Database (CSD) (organic materials)
Free Online Databases
  ICSD- 4% available as demo at http://icsd.ill.eu/icsd/index.html
  Crystallography Open Database http://www.crystallography.net/
  Mincryst http://database.iem.ac.ru/mincryst/index.php
  American Mineralogist http://www.minsocam.org/MSA/Crystal_Database.html
  WebMineral http://www.webmineral.com/
  Protein Data Bank http://www.rcsb.org/pdb/home/home.do
  Nucleic Acid Database http://ndbserver.rutgers.edu/
  Database of Zeolite Structures http://www.iza-structure.org/databases/

## Slide 13: A Crystal Structure
ZrO2
Space Group Fm-3m (225)
Lattice Parameter a=5.11
Atom | Wyckoff Site | x | y | z | Biso | sof
Zr | 4a | 0 | 0 | 0 | 1.14 | 1
O | 8c | 0.25 | 0.25 | 0.25 | 2.4 | 1
site occupancy factor, sof, is equivalent to N in the Fhkl equation

## Slide 14: Wyckoff Site notation is a shortcut to indicate if the type of site that the atoms occupies in the crystal
each letter in the Wyckoff notation specifies a site that sits on a different combination of symmetry elements
the number in the Wyckoff notation indicates the number of atoms put into the unit cell if the atom is on that site
  4a- an atom on the a site will populate the unit cell with 4 atoms
  8c- an atom on the c site will populate the unit cell with 8 atoms
  Wyckoff notation gives you a quick way to check if stoichiometry is correctly preserved when you create a crystal structure
  you can deduce z, the number of molecules per unit cell, from the Wyckoff notation (z=4 for ZrO2)
  The Wyckoff site indicates if x, y or z are can change or if they must be fixed to preserve the symmetry of the crystal

## Slide 15: The Site Occupancy Factor, sof, indicates what fraction of a site is occupied by a specific atom
The sof is N in the structure factor equation
sof = 1, every equivalent position for xyz is occupied by that atom
sof < 1, some of the sites are vacant
two atoms occupying the same site will each have a fractional sof
remember that the observed XRD pattern is an average of hundreds or thousands of unit cells that make a crystallite

## Slide 16: For pattern calculations and Rietveld refinement in HSP, the “Structures” desktop is recommended
Desktops can be changed in the menu:
  View > Desktops
All slides in this tutorial were created with HSP in the “Structures” desktop

## Slide 17: With this crystal structure information, we can build a crystal in HSP
Start X’Pert HighScore Plus
Create a New Document File>New
Analysis>Rietveld>Enter New Structure

## Slide 18: Step 1: Enter Title
Follow the entry form from top to bottom, via the numbered steps

## Slide 19: Step 2: Enter Space Group
Each space group has a unique number (1 thru 230)
  you can just enter number into the space group field
  HSP will assume the standard origin and setting
You can use the drop-down menu to select a space group
You can open the symmetry explorer by clicking on the ... button

## Slide 20: The symmetry explorer allows you to choose the space group and a specific origin, and to see information about the symmetry elements and special positions

## Slide 21: Step 3: Enter Unit Cell
lattice parameters are automatically constrained by the space group that you chose
  a cubic space group: a=b=c, a=b=g=90

## Slide 22: Step 4: Enter Atoms
The element can be an atom or ion (select oxidation state)
  the use of oxidation states in modifying the scattering factor for an atom is set in Customize>Program Settings, in the Rietveld tab
  by default it is set to “Ignore Oxidation States”
name is the element by default, but it can be changed (useful if you have the same element on multiple sites)
entering Wyckoff site can save you from having to type in xyz
  if you enter xyz, the Wyckoff site is automatically assigned
When finished, click OK to create that crystal structure!

## Slide 23: We can now simulate the ideal X-Ray powder diffraction pattern in HSP
We have entered in all of the information necessary to simulate an X-ray diffraction pattern
Click on the ‘Start Pattern Simulation’ button to produce the theoretical diffraction pattern

## Slide 24: The pattern simulation parameters can be changed in Program Settings
To change settings go to Customize> Program Settings
In Simulation tab, you can change the parameters for the simulated scan
  Default range for simulation is 5 to 70 °2theta
  change start and end angles to 25 and 90 °2theta
  click OK to enter change and close window
click ‘Start Pattern Simulation’ again

## Slide 25: The wavelength of radiation used in the simulation can be changed in Document Settings
To change settings go to Customize> Document Settings
In Document Wavelength tab, you can change the X-ray source used
  there is an “Other” option if you used a non-characteristic wavelength, such as at a synchrotron
click ‘Start Pattern Simulation’ again

## Slide 26: Parameters for the crystal structure and the simulation can be accessed in the Refinement Control list
the parameters for the pattern simulation are shown in the Refinement Control List
The values for global parameters and each individual crystal structure entered into the simulation are listed in a nested tree format
You can trim the number of tabs in the Lists Pane in the View menu

## Slide 27: The Object Inspector shows additional details for any element you select in other windows
If you click on the phase name (eg Zirconia) in Refinement Control list, you will be able to see additional information about that phase in the Object Inspector
  This includes information such as calculated density, chemical formula, and formula mass
  You can use these to check that you created the crystal structure correctly
  You can change details such as the phase name and color of simulated diffraction pattern

## Slide 28: We want to keep this pattern as a reference during the next exercises
Go to Scan List in the Lists Pane
Right Click on the current scan that is shown in the list (which is the simulated pattern)
Select “Convert calc. Profile to obs. Profile”
Now the original simulation will remain in the Main Graphics View and we can compare it to new simulations

## Slide 29: We can change parameters for the crystal structure and observe how they change the diffraction pattern
The unit cell lattice parameters determine where the diffraction peaks are observed
the peak intensity is determined by
  what atoms are in the crystal and their positions xyz
  the site occupancy of the atom
  the relative scattering strength of the atom, scattering factor, which is a product of the number of electrons around the atom
  the thermal parameter of the atom
This is not just useful for these tutorial purposes, but also for anticipating what your real data might look like and for evaluating limits of detection

## Slide 30: To change values for the simulation
In the Refinement Control,
  expand the Zirconia entry
  Expand the Unit Cell entry
  Change the Unit Cell value
    After typing, you must press ‘Enter’ key to register the change
    if you try recalculating the simulation without pressing enter, you may lose the changed value
recalculate the diffraction pattern by clicking on “Start Pattern Simulation” button again
change the lattice parameter and recalculate the pattern several times to get a feel for the relationship

## Slide 31: To change atom parameters
click on Atomic Coordinates in the Refinement Control List
The atomic information appears in the Object Inspector
Expand the Object Inspector window so that you can see more clearly
You know that you are working with the atoms because the Object Inspector pane says “Selected Object: Atomic Coordinates”

## Slide 32: Change the Site Occupancies (sof) for the atoms
Changing the occupancy of Zr has a big effect
  change the SOF of Zr to 0.5 and recalculate the pattern
Changing the occupancy of O has a small effect
  reset the SOF of Zr to 1.0 and change the SOF of O to 0.5, then recalculate the pattern
Remember, the atomic scattering factor, f0, is equal to the number of electrons around the atom
  Zr atoms scatter much more strongly than O, so the XRD diffraction pattern is more sensitive to the Zr atoms

## Slide 33: We can predict the change in peak intensities when we dope the sample
replace 20% Zr with Y
  right click on the Object Inspector and select “add new atom”
  To create the new atom, type “Y” for the Element
  tab over to Wyckoff Site and type “4a” and enter
    this automatically places the atom at 0,0,0
  make the sof 0.2
  make the Biso 1.14
  make the sof for the Zr atom 0.8
  This means that the 4a site is occupied by 80% Zr and 20%Y
  recalculate the simulation
    little change in intensity
replace 20% Zr with Ce
  change the atom type of Y to Ce and recalculate the simulation
how could we quantify amount of Y doping in YSZ?

## Slide 34: The thermal parameter, Biso, changes how scattering efficiency changes with as a function of (sin q)/l
change thermal parameter for Zr
  reset the SOF of Zr to 1 and the SOF of the other 4a atom (Ce or Y) to 0
    the diffraction pattern will be representative of ZrO2 with no doping
  change Biso and recalculate the diffraction pattern
    change from 1.14 to 2.3
    change to 5
    change to 0.1

## Slide 35: These simulations do not necessarily represent the data that your diffractometer will produce
There are more factors that contribute to the diffraction pattern that you collect with an instrument
Some of these factors are calculated from fundamental equations
  The simulations that we have been executing already account for multiplicity, for Ka2 radiation, and for the Lorentz polarization factor
Some of these factors are approximated using empirical formulas
  The simulations that we have been executing already account for the peak width due to divergence, mosaicity, resolution of the diffractometer

## Slide 36: Other Things that effect intensity
IK=SMKLK|FK|2PKAKEK
S is an arbitrary scale factor
  used to adjust the relative contribution of individual phases to the overall diffraction pattern
M is the multiplicity of the reflection
  accounts for the fact that some observed diffraction peaks are acutally the product of multiple equivalent planes diffracting at the same position 2theta (for example, (001) (100) (010) etc in cubic)
  automatically calculated based on the crystal structure
L is the Lorentz polarization factor
P is the modification of intensity due to preferred orientation
A is absorption correction
E is extinction correction
F is structure factor, which is the amplitude of scattered light due to the crystal structure (already discussed)

## Slide 37: The Lorentz polarization factor corrects for several effects
The Lorentz factor
  Different planes remain in the diffracting condition over a different angular range
  high angle planes remain in the diffracting position longer, increasing their apparent intensity
  1/sin2qcosq relationship for Bragg-Brentano
  varies with geometry of the diffractometer
Polarization
  Scattering of light by the atom polarizes the X-rays
  this causes the scattered intensity to vary as 1+cos2(2q)/2
Monochromator Polarization
  The monochromator uses diffraction from a crystal to remove unwanted wavelengths of radiation.
  This diffraction will also polarize the X-ray beam, causing intensity to vary as cos2(2q)
    POL is the correction factor for the monochromator
    the correct POL value can be found in HSP Help
      go to the Help Index, type in POL, and the first option describes the Lorentz polarization factor
Monochromator | POL
K-beta Filter | 1
Cu diffracted beam graphite (point detector) | 0.8
Cu X’Celerator | 1.25
Cr diffracted beam (point detector) | 0.588

## Slide 38: Setting the Polarization Correction Coefficient, POL, for your simulation
in the Refinement Control list, click on Global Parameters
The Global Parameters will show up in the Object Inspector
In the “General Properties” expansion of the Object Inspector, you can set the Polarization Correction Coefficient (POL)

## Slide 39: Modeling Preferred Orientation
The default calculation assumes that there are an equal number of crystallites contributing to every diffraction peak
  the orientation of the crystallites is random and there are a statistically relevant number of grains
preferred crystallographic orientation produces a non-random distribution in the orientation of the crystallites
  the observed diffraction peak intensities will vary systematically

## Slide 40: The March distribution function empirically models the preferred orientation effect
The March distribution function is a model for fitting preferred orientation of cylinder or needle shaped crystals.
k is the angle between the preferred orientation vector and the normal to the planes generating the diffracted peak
r is a refinable parameter in the Rietveld method
we will explore using the correction in our refinement on Tuesday

## Slide 41: Modeling Preferred Orientation in HSP
In the Refinement Control list, click on the phase that has preferred orientation
In the Object Inspector, expand the Preferred Orientation settings
  set the h,k, and l directions to represent the [hkl] of the preferred orientation
  set the Preferred Orientation parameter
    this parameter is found in the Object Inspector as “Parameter (March/Dollase)”
    this parameter is also found in the Refinement Control List as “Preferred Orientation”
    1 means the orientation of [hkl] is completely random
    <1 means that the [hkl] direction is the preferred orientation of the crystallites
    >1 means that the [hkl] direction is preferentially avoided
recalculate the simulation to observe the change in peak intensities

## Slide 42: Additional Intensity Factors
Absorption Correction
  accounts for the transmission and absorption of the X-rays through the irradiated volume of the sample.
  depends on sample geometry: flat plate or cylindrical
  depends on the mass absorption coefficient of the sample
    significant for cylindrical or transmission samples with a high sample absorption
    significant for a flat plate sample with a low sample absorption
Extinction Correction
  Secondary diffraction of scattered X-rays in a large perfect crystal can decrease the observed intensity of the most intense peaks
  scattering by uppermost grains limits the penetration depth of a majority of X-rays, causing a smaller irradiated volume
  want “ideally imperfect” crystals– grains with enough mosaicity to limit extinction
  better to reduce extinction by grinding the powder to a finer size
These two corrections are rarely used. Caution is advised. Always check to make sure that the correction values are physically meaningful.

## Slide 43: We now know how to calculate the diffraction peak intensity, but there a couple of more factors involved in simulating real diffraction data
The intensity, Yic, of each individual data point i is calculated using the equation:
We already know how to calculate IK, the intensity of the Bragg diffraction peak k: IK=SMKLK|FK|2PKAKEK
Yib is the intensity of the background at point i in the pattern
k1 - k2 are the reflections contributing to data point i in the pattern
  sometimes multiple Bragg diffraction peaks overlap, resulting in multiple contributions to the observed intensity at a single data point
Gik is the peak profile function
  this describes how the intensity of the diffraction peak is distributed over a range of 2theta rather than at a single point
  this profile is due to instrument broadening, sample broadening, etc

## Slide 44: Diffraction peaks have profiles that must be empirically modeled
44
Sample attributes also contribute to the diffraction peak shape and width
  mass absorption coefficient (sample transparency)
  sample thickness
  crystallite size
  microstrain
  defect concentration
The intensity equation Ik predicts that diffraction peak intensity occurs at a single point 2theta– but in reality the diffraction peak intensity is spread out over a range of 2theta
  The total area of the diffraction peak profile is the predicted intensity Ik
Diffractometers contribute a characteristic broadening and shape to the diffraction peak based on their optics and geometry
  each separate combination of divergence slit apertures, Soller slits, beta filter or monochromators, and detectors will have their own characteristic instrument profile

## Slide 45: Profile Parameters
45
Rietveld refinement assumes that peak profiles vary systematically as a function of 2theta
Peak profile may also vary according to crystallographic direction [hkl]
Peak Width
Peak Shape

## Slide 46: The Cagliotti equation describes how peak width varies with 2theta
Hk is the Cagliotti function where U, V and W are refinable parameters
HSP treats the Cagliotti equation as a convolution between instrument and sample broadening functions
The change in U and W between an instrument profile standard (eg NIST 640c) and your sample can indicate the amount of nanocrystallite size and microstrain broadening

## Slide 47: The systematic variation of peak width with 2theta
47
Notes: For a determination of the resolution, we again used the NIST Standard Reference Material SRM1976 (Aluminium Oxide; corundum) and measured this overnight from 20 to 120 degrees 2Theta. We determined the Full Widths at Half Maximum (FWHMs) of the reflections using X’Pert Graphics and Identify. We plotted all reflections with an intensity exceeding 0.5% of the largest reflection as a function of 2Theta and fitted the data points with the Cagliotti function, a well-known description of the instrumental aberrations of a powder diffractometer.
It is clear from the graph that the resolution in the diffractogram is excellent: a FWHM at the lowest reflections below 0.04 degrees 2Theta is easily obtained. We tried to obtain the same results with the traditional detection geometry: a receiving slit and a proportional counter but did not carry out the actual experiment because it would cost us more than one month of continuously scanning.
It is clear from this result that the resolution of the X’Celerator equals the traditional systems, or even improves it because it becomes possible to obtain higher-quality data in the same time as the traditional system.

## Slide 48: Diffraction Peaks from laboratory diffractometers are a mixture of Gaussian and Lorentzian profiles
48
Position [°2Theta]
45.50
46
Counts
0
1000
2000
3000
4000
Gaussian profile shape
Position [°2Theta]
42
44
46
48
50
Counts
0
1000
2000
Lorentzian profile shape

## Slide 49: Several different functions can be used to describe the mixing of Gaussian and Lorentzian contributions
The profile function is set in the Object Inspector for Global Parameters (found in Refinement Control list)
  the same profile function is used for all phases in a single pattern
  Pseudo Voigt and Pearson VII are the most commonly used
  Pseudo Voigt
  Pseudo Voigt with FJC Asymmetry correction
  Pearson VII
  Voigt

## Slide 50: The Pseudo Voigt equation uses up to 3 parameters to describe Gaussian and Lorentzian components
The parameters g1, g2, and g3 are the refinable shape parameters, listed as Peak Shape 1, Peak Shape 2, and Peak Shape 3 in the Refinement Control list
  Usually Peak Shape 1 is the only one used
Hk is the Cagliotti peak width function
C1 is 4 ln 2
Xkj is

## Slide 51: Background can be empirically fit with an equation, manually fit, or evaluated with blank
51
refinement of a polynomial function
refinement using a type I or II Chebyshev polynomial function
By amorphous sinc function
linear interpolation between base points
independent data collection run without the sample in place

## Slide 52: Systematic error in diffraction peak positions can also be calculated
The systematic error functions are found in Global Parameters
They apply to all phases in the sample
  zero shift
  specimen displacement

## Slide 53: The Parameters of a Pattern Simulation
53
Global parameters affect the entire sample rather than individual phases
  Background function
  Zero Shift
  Specimen Displacement
  POL (lorentz polarization factor)
  Sample Geometry
  selecting the Profile Function
Other parameters are set individually for each phase
  scale factor
  preferred orientation (March-Dollase function)
  unit cell
  atomic parameters are for each atom in the phase
    position, SOF, thermal parameter
  Peak Profile parameters
    Cagliotti peak width function parameters U,V, and W
    Profile shape parameters
    peak asymmetry profile
    anisotropic broadening function

## Slide 54: What is Physically Meaningful?
Wel (1975)
54