Experimental part

Transmission electron microscopy (TEM) under 200 kV was also performed on thin foils for the specimen homogeneized at 1200°C for 2 days, austenised at 950°C for 30 minutes under argon and isothermally held at 250°C for 16 h. Thin foils were ground to 50 μm and finally electrochemically thinned using a Struers Electropol twin jet polishing system so that they become electron transparent. The electrolyte was a solution composed in volume of 5% perchloric acid, 15% glycerol and 80% of methanol. The thinning was done under 32 V (22.5 V) at -34°C (-17.7°C), i.e. under a 5.7 A/mm² (3.2 A/mm²) current density, for the not tempered (tempered at 500°C for 1 day) specimen until a fine perforation was obtained.

Results

Figure X shows the microstructure of the untempered specimen homogeneized at 1200°C for 2 days, austenised at 950°C for 30 minutes under argon and isothermally held at 250°C for 16 h. The selected area electron diffraction (SAED) pattern proves the existence of two slightly misorientated bainitic ferrite lattices (red bold dotted lattice and yellow continuous lattice in figure Xb). Figure Xc shows an example of dark field image corresponding to the red encircled spot in figure Xb. This picture highlights the thin plated structure of bainitic ferrite.  The SAED pattern also puts into evidence the existence of another slightly larger lattice (green bold dotted-dashed lattice in figure Xb) which corresponds to the austenite phase. The latter phase is very likely intercalated between the thin plates of bainitic ferrite.

| a | b |
| --- | --- |
| c | d |

Figure X: Inner microstructure of the specimen isothermally held at 250°C for 16h without tempering (BF micrograph) (a). SAED pattern of figure a (b); DF micrograph corresponding to the red encircled spot in figure b (c); magnification of figure b (d).

The red bold dotted and yellow continuous lattices correspond to the [111] zone axis of bainitic ferrite whereas the green bold dotted-dashed lattice has been identified as the [110] zone axis of austenite.

Figure Y depicts the effect of tempering on the microstructure of the specimen isothermally held at 250°C for 16h. Both samples are globally constituted of bainitic ferrite plates. Nevertheless the thickness of the bainitic ferrite plates has changed as proved in the following.

Figure Y: Inner microstructure of the specimen isothermally held at 250°C for 16h without tempering (a) and with tempering at 500°C for 1 day (b).

In a normal direction to the length of the bainitic ferrite plate, equation 1 enables to evaluate the true thickness of the plates (t).

LTα= t/2 				[Equation 1]

with LTα: mean lineal intercept [3].

The dimensionless error of mean lineal intercept is given by equation 2.

[E(LTα)]² = 1/N * [L / LTα]²				[Equation 2]

with L standard deviation of the intercepts, N the number of measurements and E(LTα) the dimensionless uncertainty [10].

The error on the true thickness is then deduced by using equation 3.

E(t) = 2*G(LTα)/ 					[Equation 3]

with G(LTα) the uncertainty i.e. E (LTα) multiplied by the mean lineal intercept twice so as to have 95% confidence.

With equations 1 to 3, it is possible to deduce the true thickness of the bainitic ferrite plates.

With regard to the specimen isothermally held at 250°C for 16 h, the true thickness of the plates (t) is close to 38  3 nm from 100 measurements of lineal intercepts for the untempered sample vs. 43  4 nm from 55 measurements of lineal intercepts for the tempered one at 500°C for 1 day. These values of true thickness are quite similar and typical of a superbainitic structure.

The comparison of figures Ya and Yb further shows that instead of austenite at the interface of the bainitic ferrite plates, some fine carbides have precipitated during tempering at 500°C for 1 day. According to formula described in literature [11, 12] and to the analysis of 182 precipitates, the volume fraction and the interspacing of precipitates with a mean radius of 5.8 nm, assuming that they are equiaxed, were estimated to 2.47% and 60 nm, respectively.  These calculations were performed reasonably supposing that the thin foil was 50 nm thick.

Discussion

In order to understand the effect of tempering on the mechanical properties of the samples, some calculations were performed so as to evaluate the yield strength of the untempered and tempered samples. Concerning the various strengthening contributions of a sample, they can be expressed by equation 4 as follows [13-14]:

σ=σFe+iσSS,i+σC+115×LTα−1+7.34×10−6×ρD+335fλ		[Equation 4]

with SS,i = 85 %Si + 32 %Mn + 30 %Mo -30 %Cr [15-16] and C = 1722.5 %C with %C: the carbon content in solid solution in the bainitic ferrite [13].

Fe is the strength of pure annealed iron, SS,i the solid solution strengthening due to substitutionnal solute i, C the solid solution due to carbon, LTα mean lineal intercept of bainitic ferrite plates, D the dislocation density, f the volume fraction and  the distance between any carbide particles. Nevertheless the 335 factor was checked for a 0.07-0.4% carbon content range in steel [14].

Table X summarizes the different strengthening contributions for the specimen isothermally held at 250°C for 16h and eventually tempered at 500°C for 1 day. The difference between both samples is mainly due to the contribution of both the dislocations and the thickness of the bainitic ferrite plates. The calculations indeed show that the strengthening of carbides is very low in the tempered sample since their interspacing (60 nm) is about 6 times greater than their size (11.6 nm). The values resulting from the sum of the different contributions are of the same order of range as the experimental ones, although they are slightly greater. The calculations confirm that the yield strength of the tempered sample is lower than the untempered specimen one’s, as shown in figure Z.

Table X: Effect of tempering on the respective contributions of various factors to the strengthening of the specimen isothermally held at 250°C for 16h.

| Strengthening contributions (MPa) | Untempered specimen | Tempered specimen |
| --- | --- | --- |
| Solid solution of C and alloying elements | 476.2 | 476.2 |
| Thickness of the bainitic ferrite plates | 1916.7 | 1691.2 |
| Dislocations | 582.6 * | 0.1 * |
| Carbides | 0 | 9.4 10-10 ** |
| Fe | 168.0 | 168.0 |
| Sum of the contributions (MPa) | 3143.4 | 2335.4 |

* A dislocation density has been assumed to be equal to 6.3 1015/m² for the untempered sample [13] and to 108/m² for the tempered one.

** A 50 nm thin foil has been considered for the calculations.

References

3	C. Garcia-Mateo, F.G. Caballero, H.K.D.H. Bhadeshia

Acceleration of low temperature bainite

ISIJ International 43(11) (2003) 1821-1825

10	H.K.D.H. Bhadeshia

Introduction to quantitative metallography

Materials Science & Metallurgy, Part II: Metallography

11	J.W. Cahn, J. Nutting, Transmission Quantitative Metallography, Transactions of the Metallurgical Society of AIME, Vol. 215 (1959) 526-528

12	G. Frommeyer, in R.W. Cahn and P. Haasen (eds) Physical Metallurgy, Vol. 2 (1983) 1858

13	C.H. Young, H.K.D.H. Bhadeshia, Strength of mixtures of bainite and martensite, Materials Science and Technology Vol. 10 (1994) 209-214

14	J. Daigne, M. Guttmann, J.P. Naylor, The influence of lath boundaries and carbide distribution on the yield strength of 0.4% C tempered martensitic steels, Materials Science and Engineering 56 (1982) 1-10

15 	F.B. Pickering, T. Gladman, Metallurgical developments in carbon steels no. 81. Iron and Steel Inst. Spec. Rep. (1963) 10

16	G. R. Speich, H. Warlimont, Yield strength and transformation substructure of low carbon martensite. J. Iron and Steel Inst. 206 (1968) 385-392