Table 7: Nanohardness values and standard error of the WEM and matrix of sample MPC using a constant indentation depth of 1000 nm.

|  |  |
| --- | --- |
| Region | Nanohardness / GPa |
| WEM | 12.3±0.2 |
| Matrix | 11.3±0.6 |