## Slide 1
(a)
(b)
(c)
1 K s-1
3 K s-1
20 K s-1
100 K s-1
Cooling
(d)
Figure 1: Heat treatment patterns (a) A, (b) B, (c) C, (d) dilatation curves.

## Slide 2
Fe 703
P 120
C 271
(b)
50 ㎛
(a)
(b)
(c)
Figure 2: (a) Fracture surface of AES sample cooled at 1 K s-1 according to pattern A in
Fig. 1, (b) Spectrum from intergranular surface, (c) Spectrum from cleavage facet.
Fe 703
(c)

## Slide 3
Figure 3: (a) Thermal grooves as well as oxide-etching reveal the austenite grain boundaries;
(b) The same sample, lightly polished and lightly etched with nital, to reveal the ferrite grain boundaries and vestiges of the austenite grain boundary grooves. Note that the two figures are not from the same locality, and that the arrows in (b) indicate the austenite grain boundaries revealed by the thermal grooving that remains following light polishing and etching to reveal the ferrite grain boundaries.
(a)
(b)

## Slide 4
Figure 4: Grain size of ferrite according to the heat treatment conditions.
100
20
3
1
Grain size (μm)

## Slide 5
Figure 5: Atomic fraction of phosphorous in grain boundary (a) pattern A, (b) pattern B,
(c) pattern C, (d) optical microstructure of specimen cooled at 400 K s-1.
400
100
20
3
1
100
20
3
1
100
20
3
1
(a)
(b)
(c)
(d)

## Slide 6
Figure 6: Comparison between average distance of interface migration (grey points) during the transformation and diffusion distance of phosphorous. The curve is calculated using grain boundary diffusivity where the flux is parallel to the boundary.
Cooling rate (K s-1)
Distance (μm)