## Slide 1
Sample | Cooling rate (K s−1) | Atomic fraction P | 95 % confidence interval
Fig. 5a | 400 | 0.11752 | 0.01602
Fig. 5a | 100 | 0.12969 | 0.0154
Fig. 5a | 20 | 0.13167 | 0.01167
Fig. 5a | 3 | 0.14853 | 0.01411
Fig. 5a | 1 | 0.14643 | 0.01258
Fig. 5b | 100 | 0.12969 | 0.0154
Fig. 5b | 20 | 0.12896 | 0.01544
Fig. 5b | 3 | 0.1257 | 0.01404
Fig. 5b | 1 | 0.12997 | 0.01265
Fig. 5c | 100 | 0.12997 | 0.01265
Fig. 5c | 20 | 0.13535 | 0.00923
Fig. 5c | 3 | 0.14512 | 0.01215
Fig. 5c | 1 | 0.14643 | 0.01258
Table 1: Quantitative data relating to Fig. 5.

## Slide 2
 | Cooling rate from Tγ = 1373 K |  |  | 
 | 100 K s−1 | 20 K s−1 | 3 K s−1 | 1 K s−1
Pattern B, segregation during γ → α change, xB | 0.130 | 0.129 | 0.126 | 0.130
Segregation during cooling below Tf , xA ‒ xB | 0 | 0.003 | 0.022 | 0.016
Table 2: Segregation of phosphorous during and after phase transformation
Concentrations x are presented as atomic fractions.
 | 100 K s−1 | 20 K s−1 | 3 K s−1 | 1 K s−1
Segregation during γ → α change during cooling at 1 K s−1 | 0.130 | 0.130 | 0.130 | 0.130
Segregation during cooling at different rates below Tf , xC ‒ 0.13 | 0 | 0.005 | 0.015 | 0.016
Table 3: Segregation of phosphorous during phase transformation and cooling in ferrite regime estimated from AES analysis on heat treatment pattern C.