## Slide 3
Robert Hooke, Micrographia, 1665
Sche:VII

## Slide 4: Phase transitions
ice: pure
ocean: salty water
photograph courtesy of Sunita Hansraj from her Antarctica expedition
Harry Bhadeshia
Haixue Yan
Phase transformations

## Slide 5: Definition of a phase

## Slide 6
crystalline
NASA image S72-552082

## Slide 7: Anisotropy elastic modulus / GPa
Ag
Mo

## Slide 8: liquid to glass transition
amorphous

## Slide 9
anisotropic molecules
solid crystal, ordered
liquid crystal,
somewhat ordered
liquid: cannot support
shear stress

## Slide 10: A transformation: change in atomic arrangement.
….. by breaking all original bonds and making new ones
….. by deformation into a new pattern

## Slide 11
reconstructive transformation
diffusion
change in composition
minimal strain energy
close to equilibrium

## Slide 12
Low atomic mobility:
all atoms

## Slide 13
displacive transformation
diffusionless
no change in composition
large strain energy
far from equilibrium

## Slide 14: Problem 1
Elastic modulus = 200 GPa

## Slide 15: Problem 2
Elastic modulus = 200 GPa

## Slide 16
J. H. Pak, D. W. Suh, H. K. D. H. Bhadeshia
Metall. & Mater. Trans A 43 (2012) 4520
Real time
|
|
50 µm
thermally induced, steel

## Slide 17
one condition for diffusionless growth

## Slide 19: martensite

## Slide 20
IPS: invariant-plane strain

## Slide 23
Sufficient atomic mobility
Reconstructive
transformation

## Slide 24: Phenomenological interpretation of reconstructive transformation

## Slide 26: Transformation of a phase

## Slide 27: Transformation of a phase
magnetic fields
field measured in Teslas
Nikola Tesla
QMUL-SEMS laboratory 136
field strength at Earth's magnetic equator is 0.0000305 Tesla.
We can do experiments using 10 Tesla.

## Slide 28: Why does a change in temperature sometimes cause a change in phase? Why … change in magnetic field …

## Slide 29
How to detect change in phase: one method, diffraction

## Slide 30
Bragg equation: constructive interference

## Slide 31
Desktop X-ray diffraction equipment

## Slide 32: Shielding

## Slide 33
X-ray diffraction

## Slide 34: European synchrotron facility

## Slide 35
Symmetrical
Symmetrical
Not symmetrical

## Slide 36: Real-time sequence
Diffraction angle 2θ
Intensity
H. J. Stone, M. J. Peet, H. K. D. H. Bhadeshia, P. J. Withers, S. S. Babu, E. D. Specht
Proc. of the Royal Society A, 464 (2008) 1009-1027

## Slide 37: orthogonal axes

## Slide 38: Barium titanate

## Slide 39
Lattice parameter of cubic form = 0.404 nm

## Slide 40: Cubic barium titanate

## Slide 42: Tetragonal barium titanate

## Slide 43
no centre of symmetry
ferroelectric
piezoelectric
pyroelectric

## Slide 44: First ceramic microphone, 1957, barium titanate
convert mechanical vibrations into electrical signals

## Slide 45: Atomic force microscopy
control such tiny movements using peizoelectric devices

## Slide 46: Imagine barium titanate inside the human body
can electrically stimulate tissue
without an external power source
high biocompatibility (absence of inflammation or foreign body responses)
However, no difference between electrically stimulated and inactive implants

## Slide 47: Reversible if no damage accumulated
magnetically-induced, Ni-24Mn-24Ga at.%
Professor Koichi Tsuchiya
Toyohashi University of Technology, Japan.

## Slide 48
Olson and Hartman, 1982

## Slide 49
Olson and Hartman, 1982

## Slide 50
Olson and Hartman, 1982