## Slide 2: Phase transitions elementary thermodynamics
Harry Bhadeshia
Haixue Yan
photograph courtesy of Sunita Hansraj from her Antarctica expedition
“many observable properties so that they can be seen to be a consequence of a few”

## Slide 3: Internal energy
measure of total energy of all particles in substance
includes kinetic energy
includes chemical potential energy due to bonds

## Slide 4: change in internal energy
heat added and work done by the system are positive

## Slide 6
pendulum at any instant has kinetic and potential energy
For a molecule stimulated by thermal energy, .........

## Slide 7
Notes: for alpha and gamma, Debye temperatures about 400 K

## Slide 10
many components to heat capacity

## Slide 11: differential scanning calorimetry

## Slide 12: differential scanning calorimetry

## Slide 14: Problem: what is happening at arrows ? exothermic or endothermic?

## Slide 16: reactions happen whether they absorb or emit heat

## Slide 17: consider ideal gas
ordered
disordered

## Slide 18
Chart: Temperature / °C

## Slide 19
reaction spontaneous only if

## Slide 20: configurations
essentially means “arrangements”
some more probable than others

## Slide 22: Problem: How many distinguishable ways can these atoms be arranged on lattice?
lattice
atoms
2 configurations

## Slide 23
lattice
atoms
1 configuration
Problem: How many distinguishable ways can these atoms be arranged on lattice?

## Slide 24
1
1
2
1,2
2,1
1
2
3
1,2,3
1,3,2
2,1,3
2,3,1
3,2,1
3,1,2

## Slide 25
+

## Slide 26
logarithm of large number

## Slide 31
displacive transformation products are stopped at parent grain boundaries

## Slide 35
metallic glass

## Slide 36
domain boundaries
glass: no structure
∴ magnetically soft

## Slide 37: Wish to know melting temperature of a five-component system (Fe,Mn,Al,Au,Mg). What are the variables?
concentration
crystal structure
pressure

## Slide 38: have thermodynamic data, e.g.,
how “energy” of each element varies with temperature
how “energy” of each element, changes with its structure
how these “energies” change when elements mixed – models for mixtures

## Slide 39: Crystal structures at high temperatures
Fe, Mn
Au, Al
Mg

## Slide 40: melting temperature Fe+Au+Mn+Al+Mg
 | Tm / K
Fe | 1811
Fe-4Au wt% | 1793
Fe-4Au-4Mg | 723
Fe-4Au-4Mn | 1763
Fe-4Au-4Mn-4Al | 1763
calculations in steps of 10 K,
only liquid and BCC allowed to exist

## Slide 41
melting temperature of hexagonal Mg = 923 K

## Slide 43
heat transfer permitted in both cases
closed system allows transfer of heat but not mass