## Slide 1
courtesy of T. DebRoy

## Slide 2: Crystal structure?
equiatomic Cr Mn Fe Co Ni

## Slide 3
Parker Beatty
Creative Commons Attribution-Share Alike 4.0 International

## Slide 5
There are many industrial processes where we mix powders rather than atoms.
Ball milling is used to make strange alloys where powders really don’t want to mix, but we force them to do so and form an atomic solution.
The purpose is to achieve properties never before achieved.
an application of thermodynamics

## Slide 6
extrusion of canned powder
image courtesy of Jan-Olof Nilsson
Sandvik Materials Technology.
Extrusion of stainless steel.

## Slide 7
an application of thermodynamics
Suppose that instead of atoms, we mix particles of A and B, each containing many atoms
What is the configurational entropy of mixing?

## Slide 8
For a random mixture of particles, number of configurations given by:

## Slide 10
Solution-like behaviour when particles about 1000 atoms in size
Free energy of mixing due to configurational entropy alone

## Slide 11: How do we know that an atomic solution has formed?

## Slide 12
Chou & Bhadeshia

## Slide 14
Probability of pairwise bonds in random solution

## Slide 15: Phase transitions equilibrium state
photograph courtesy of Sunita Hansraj from her Antarctica expedition
“nothing changes, no matter how long it is observed”
stable to infinitesimal perturbation

## Slide 16: transformation without composition change

## Slide 17
pure iron

## Slide 18
Solutions

## Slide 20: chemical potential

## Slide 21
ice: pure
ocean: salty water
photograph courtesy of Sunita Hansraj from her Antarctica expedition
two solutions in contact
compositions different, yet in equilibrium

## Slide 24: proportions of phases: lever rule

## Slide 25: Liquid can decompose simultaneously into two solids

## Slide 26
Simulation, Britta Nestler, RWTH Aachen

## Slide 27: eutectic
Edo Museum in Tokyo. Shogun era, about 130 years ago.
Melting temperatures
Lead 328°C
Tin 232°C
Pb-62Sn wt% 183°C

## Slide 28
eutectic
hypereutectic
hypoeutectic

## Slide 29: Why eutectic?

## Slide 37
images courtesy of
Jane Weston

## Slide 38
constant temperature section
ternary phase diagram

## Slide 39: What do we need from phase diagrams?
stable phases
fractions of phases
compositions of phases
as a function of temperature, pressure etc.
consider 7 components (Fe, C, Si, Mn, Ni, Mo, Cr)
three phases BCC, Fe3C, M23C6

## Slide 42
Condition for equilibrium is simple:
uniform chemical potential defines equilibrium

## Slide 44
Praseodymium-neodymium solid solutions
Lundin, Pool: J. Less Common Metals 9 (1965) 48-53

## Slide 45
configurational entropy maximum at equiatomic concentration
free energy minimum at equiatomic concentration, assuming only the entropy contributes to free energy
1000 K

## Slide 46: “regular” solution
change in bond energy when AA and BB bonds replaced in part by AB and BA bonds

## Slide 50: Create solution by mixing in proportion
A
B
solution
number of A atoms
number of B atoms
total number of A+B atoms

## Slide 51
A
B
solution
number
A-A bonds?
number
B-B bonds?

## Slide 55
Parlier M, Valle R, Perrière L, Lartigue-Korinek S, Mazerolles L. Potential of directionally solidified eutectic ceramics for high temperature applications. Aerospace Lab. 2011 Nov 1(3):p-1.