## Slide 1: Phase transitions equilibrium state
photograph courtesy of Sunita Hansraj from her Antarctica expedition
“nothing changes, no matter how long it is observed”
stable to infinitesimal perturbation

## Slide 2: transformation without composition change

## Slide 3: chemical potential

## Slide 8: lever rule

## Slide 9: lever rule

## Slide 10: Modern pewter: tin with Cu, Sb, Bi

## Slide 11: eutectic
Edo Museum in Tokyo. Shogun era, about 130 years ago.
Melting temperatures
Lead 328°C
Tin 232°C
Pb-62Sn wt% 183°C

## Slide 12
eutectic
hypereutectic
hypoeutectic

## Slide 14
Simulation, Britta Nestler, RWTH Aachen

## Slide 15: Why eutectic?
,

## Slide 16
Parlier M, Valle R, Perrière L, Lartigue-Korinek S, Mazerolles L. Potential of directionally solidified eutectic ceramics for high temperature applications. Aerospace Lab. 2011 Nov 1(3):p-1.

## Slide 19
images courtesy of
Jane Weston

## Slide 20
ternary phase diagram

## Slide 22
quaternary
system

## Slide 23: What do we need from phase diagrams?
stable phases
fractions of phases
compositions of phases
as a function of temperature, pressure etc.
consider 7 components (Fe, C, Si, Mn, Ni, Mo, Cr)
three phases BCC, Fe3C, M23C6

## Slide 26
Condition for equilibrium is simple:
uniform chemical potential defines equilibrium

## Slide 28: ideal solution: random mixture of atoms concentration of `A’ atoms = (1-x)
no enthalpy of mixing
only entropy of mixing

## Slide 29
Praseodymium-neodymium solid solutions
Lundin, Pool: J. Less Common Metals 9 (1965) 48-53

## Slide 30
configurational entropy maximum at equiatomic concentration
free energy minimum at equiatomic concentration, assuming only the entropy contributes to free energy
1000 K

## Slide 31: “regular” solution
change in bond energy when AA and BB bonds replaced in part by AB and BA bonds

## Slide 36
A
B