## Slide 1: Phase transitions Nucleation
Harry Bhadeshia
Haixue Yan
photograph courtesy of Sunita Hansraj from her Antarctica expedition

## Slide 2: Nucleation of  from 
Driving force G < 0
At T = Te,

## Slide 3: Homogeneous nucleation
r*

## Slide 4: Strain energy is a barrier for the transition

## Slide 5: The nucleation rate per unit volume
Iv: the nucleation rate per unit volume
: the frequency to overcome the activation barrier
Nv: the number of nucleation sites per unit volume
k and T: the Boltzmann constant and the absolute temperature respectively.

## Slide 6
T = Te-T
G*
or
r*
G*
r*
Temperature, T
Size & free energy of formation
of critical nucleus decreases as
temperature falls

## Slide 7: Rate of nucleation vs. DT
When numbers are inserted, theory predicts that significant nucleation rates require supercooling of at least 0.2Tm, e.g.
In practice, nucleation occurs at very much smaller DT ( 0.02Tm, i.e. tens of degrees, not hundreds, below Tm).
Supercoolings ~0.2Tm are only obtained in, e.g. dispersions of very fine droplets where foreign bodies/impurities are excluded by the smallness of the volume.
Iv
DT
Effective nucleation temperature
Metal | Tm, K | 0.2Tm
Pb | 600 | 120
Ag | 1233 | 247
Cu | 1356 | 271
Fe | 1803 | 361
Tm
DT
Tg
Nucleation control
Transport control
Nucleation Rate, I

## Slide 8: Heterogeneous nucleation
At equilibrium,
As before, DG of nucleation involves surface & volume terms:
  1) top surface area of the sphere cap = 2pr2(1-cos q)
  2) Flat surface area of the sphere cap = pr2(1-cos2q)
  3) Volume of the crystal nucleus Vn= pr3(2-3cosq+cos3q)/3

## Slide 9
At r = r*
0
DT
~0.2Tm
~0.02Tm
I
Homo.
Het.
Note: as q = 180°, G*(het) = G*(hom)
Hom. nucleation is a special case of het. nucleation.

## Slide 10: Solidification: Nucleation Types
Homogeneous nucleation
  nuclei form in the bulk of liquid metal
  requires considerable supercooling (typically 80-300ºC)
Heterogeneous nucleation
  much easier since stable “nucleating surface” is already present — e.g., mold wall, impurities in liquid phase
  only very slight supercooling (0.1-10ºC)

## Slide 13: PBL one
Calculate the critical size for homogeneous and heterogeneous nucleation. In terms of their nucleation barriers G (free energy), why is homogeneous model a special case of heterogeneous model?