## Slide 1: Phase transitions Solidification
Harry Bhadeshia
Haixue Yan
photograph courtesy of Sunita Hansraj from her Antarctica expedition

## Slide 2: The velocity  of the transformation from L to S
Below the equilibrium melting temperature Tm
 (m/s)  T

## Slide 3: Solidification of Pure Metals
Liquid & solid have only one possible composition. Thus crystal growth in a pure metal is controlled only by flow of heat away from the interface.
Temperature Gradient, G (K/m)
Case I: (GS >) GL > 0 Here the solid is a better conductor of heat than the liquid, leading to a positive GL
The interface is usually at a temperature just below Tm. If a protuberance forms at a growth face,
Solid Liquid Interface
T
GS
GL
Tlocal > Tm & tip re-melts
Thus growth front remains planar: planar or columnar growth (the growth is relatively ‘stable)
S
L

## Slide 4
Case II: (GS > 0) GL < 0 This situation exists during the initial stages of nucleation when a ‘large’ supercooling is involved to initiate nucleation.
Solid Liquid Interface
T
GS
GL
Tm
Stable protuberance
Dendritic growth by repetition
S
S
S
L
L
L
If the melt is significantly supercooled, Tmelt < Tm by many °C, then the latent heat of crystallisation warms up the interface so that GL is negative.

## Slide 6: Effect of Casting Conditions
Alloy Content
Pouring Temperature
Cooling Rate

## Slide 8: Ex: Cooling of a Cu-Ni Alloy
wt% Ni
20
120
0
130
0
3
0
4
0
5
0
110
0
L (liquid)
a
(solid)
L
+
a
L
+
a
T(ºC)
A
35
C0
L: 35wt%Ni
Cu-Ni
system
• Phase diagram:
Cu-Ni system.
Adapted from Fig. 9.4, Callister & Rethwisch 8e.
• Consider
microstuctural
changes that
accompany the
cooling of a
C0 = 35 wt% Ni alloy
46
35
43
32
a: 43 wt% Ni
L: 32 wt% Ni
B
a: 46 wt% Ni
L: <35 wt% Ni
C
E
L: 24 wt% Ni
a: 36 wt% Ni
24
36
D

## Slide 9: Cored vs Equilibrium Structures
• Slow rate of cooling:
Equilibrium structure
• Fast rate of cooling:
Cored structure
First a to solidify:
46 wt% Ni
Last a to solidify:
< 35 wt% Ni
• Ca changes as we solidify.
• Cu-Ni case:
First a to solidify has Ca = 46 wt% Ni.
Last a to solidify has Ca = 35 wt% Ni.
Uniform Ca:
35 wt% Ni

## Slide 11
Non-equilibrium solidification

## Slide 12
Constitutionally supercooling

## Slide 13
In the PRESENCE of C.S. planar interface become unstable due to an increase in the level of C.S. from the interface to a distance in the melt where max. C.S. in encountered. At relatively low C.S., a cellular growth front develops.
As C.S. increases, the cells ‘caps’ becomes extended & eventually branch to form dendrites. No clear transition from cellular to dendritic growth.

## Slide 14
PBL two:
Show the equation below and discuss the effect of parameters on constitutional supercooling