## Slide 1: Phase transitions The iron-carbon system
Harry Bhadeshia
Haixue Yan
photograph courtesy of Sunita Hansraj from her Antarctica expedition

## Slide 2
ISSUES TO ADDRESS...
• Transforming one phase into another takes time.
• How does the rate of transformation depend on
time and temperature?
• Is it possible to slow down transformations so that non-equilibrium structures are formed?
• Are the mechanical properties of non-equilibrium
structures more desirable than equilibrium ones?
Fe
g
(Austenite)
Eutectoid
transformation
C
FCC
Fe3C
(cementite)
a
(ferrite)
+
(BCC)

## Slide 3: Fe-C True Equilibrium Diagram
1600
1400
1200
1000
800
600
400
0
1
2
3
4
90
L
g
+L
 + Graphite
Liquid +
Graphite
(Fe)
C, wt% C
0.65
740ºC
T(ºC)
 + Graphite
100
1153ºC
g
Austenite
4.2 wt% C
a + g
Adapted from Fig. 11.2, Callister & Rethwisch 8e.
[Fig. 11.2 adapted from Binary Alloy Phase Diagrams, 2nd ed.,
Vol. 1, T.B. Massalski (Ed.-in-Chief), ASM International, Materials Park, OH, 1990.]
Graphite formation promoted by
Si > 1 wt%
slow cooling
Fe3C  3Fe (-ferrite) + C (graphite)
Cementite Fe3C is a metastable compound.

## Slide 4: Transformations & Undercooling
•
For transf. to occur, must
cool to below 727ºC
(i.e., must “undercool”)
•
Eutectoid transf. (Fe-Fe3C system):
g
Þ
a
+
Fe3C
0.76 wt% C
0.022 wt% C
6.7 wt% C
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+Fe3C
a
+Fe3C
L+Fe3C
d
(Fe)
C, wt%C
1148ºC
T(ºC)
a
ferrite
727ºC
Eutectoid:
Equil. Cooling: Ttransf. = 727ºC
DT
Undercooling by Ttransf. < 727C
0.76
0.022
Adapted from Fig. 9.24,Callister & Rethwisch 8e. (Fig. 9.24 adapted from Binary Alloy Phase Diagrams, 2nd ed., Vol. 1, T.B. Massalski (Ed.-in-Chief), ASM International, Materials Park, OH, 1990.)

## Slide 5: The Fe-Fe3C Eutectoid Transformation
Coarse pearlite  formed at higher temperatures – relatively soft
Fine pearlite  formed at lower temperatures – relatively hard
• Transformation of austenite to pearlite:
Adapted from Fig. 9.15, Callister & Rethwisch 8e.
g
a
a
a
a
a
a
pearlite
growth
direction
Austenite (g)
grain
boundary
cementite (Fe3C)
Ferrite (a)
g
• For this transformation,
rate increases with
[Teutectoid – T ] (i.e., DT).
Adapted from Fig. 10.12, Callister & Rethwisch 8e.
675ºC
(DT smaller)
0
50
y (% pearlite)
600ºC
(DT larger)
650ºC
100
Diffusion of C
during transformation
a
a
g
g
a
Carbon diffusion

## Slide 6: Generation of Isothermal Transformation Diagrams Time-Temperature-Transformation (TTT) Diagrams
Adapted from Fig. 10.13,Callister & Rethwisch 8e. (Fig. 10.13 adapted from H. Boyer (Ed.) Atlas of Isothermal Transformation and Cooling Transformation Diagrams, American Society for Metals, 1977, p. 369.)
• The Fe-Fe3C system, for C0 = 0.76 wt% C
• A transformation temperature of 675ºC.
100
50
0
1
10
2
10
4
T = 675ºC
y,
% transformed
time (s)
400
500
600
700
1
10
10
2
10
3
10
4
10
5
0%pearlite
100%
50%
Austenite (stable)
TE (727ºC)
Austenite
(unstable)
Pearlite
T(ºC)
time (s)
isothermal transformation at 675ºC
Consider:

## Slide 7: Austenite-to-Pearlite Isothermal Transformation
• Eutectoid composition, C0 = 0.76 wt% C
• Begin at T > 727ºC
• Rapidly cool to 625ºC
• Hold T (625ºC) constant (isothermal treatment)
Adapted from Fig. 10.14,Callister & Rethwisch 8e. (Fig. 10.14 adapted from H. Boyer (Ed.) Atlas of Isothermal Transformation and Cooling Transformation Diagrams, American Society for Metals, 1997, p. 28.)
400
500
600
700
0%pearlite
100%
50%
Austenite (stable)
TE (727ºC)
Austenite
(unstable)
Pearlite
T(ºC)
1
10
10
2
10
3
10
4
10
5
time (s)
g
g
g
g
g
g

## Slide 8
On cooling the g must begin to transform as soon as it enters the g + a phase field.
Pro-eutectoid a is formed on the prior g grain boundaries;
On cooling to the eutectoid temperature, the remaining g (which now has the eutectoid composition) transforms to pearlite.
microstructure consists of both proeutectoid ferrite and pearlite.
Hypoeutectoid compositions <0.76 wt%C
Notes: If the composition is above/below the eutectoid what is this called?
The diagram shows allotriomorphic ferrite. This nucleates at the austenite grain boundary. Diffusion along the grain boundaries is faster and the shape is determined by shape of the austenite grain boundaries. 1D growth (normal to the grain boundary plane)
It is possible to form idiomorphic ferrite. This nucleates inside the grain (normally at an inclusion – a non-metallic inclusion). These grains will exhibit crystallographic facets and will typically be equiaxed.
You should be able to understand how to use the phase diagram to show that the composition of the austenite is at the eutectoid composition at the eutectoid temperature.
hypoeutectoid [haɪpəʊjʊ(:)'tektɔɪd]

## Slide 9
Hypereutectoid compositions >0.76wt%C
On cooling the g must begin to transform as soon as it enters the g + Fe3C phase field.
Pro-eutectoid Fe3C is formed on the prior g grain boundaries.
On cooling to the eutectoid temperature, the remaining g (which now has the eutectoid composition) transforms to pearlite .
microstructure consists of both Fe3C and pearlite.

## Slide 10: Bainite: Another Fe-Fe3C Transformation Product
10
10
3
10
5
time (s)
10
-1
400
600
800
T(ºC)
Austenite (stable)
200
P
B
TE
0%
100%
50%
A
A
• Bainite:
-- elongated Fe3C particles in a-ferrite matrix
-- diffusion controlled
• Isothermal Transf. Diagram, C0 = 0.76 wt% C
Adapted from Fig. 10.18, Callister & Rethwisch 8e.
Adapted from Fig. 10.17, Callister & Rethwisch 8e. (Fig. 10.17 from Metals Handbook, 8th ed., Vol. 8, Metallography, Structures, and Phase Diagrams, American Society for Metals, Materials Park, OH, 1973.)
Fe3C
(cementite)
5 mm
a
(ferrite)
100% bainite
100% pearlite

## Slide 11: Spheroidite: Another Microstructure for the Fe-Fe3C System
• Spheroidite:
-- Fe3C particles within an a-ferrite matrix
-- formation requires diffusion
-- heat bainite or pearlite at temperature just below eutectoid for long times
-- driving force – reduction
of a-ferrite/Fe3C interfacial area
Adapted from Fig. 10.19, Callister & Rethwisch 8e. (Fig. 10.19 copyright United States Steel Corporation, 1971.)
60 m
a
(ferrite)
(cementite)
Fe3C

## Slide 12: Martensite: A Nonequilibrium Transformation Product
• Martensite:
-- g(FCC) to Martensite (BCT)
Adapted from Fig. 10.21, Callister & Rethwisch 8e. (Fig. 10.21 courtesy United States Steel Corporation.)
Adapted from Fig. 10.20, Callister & Rethwisch 8e.
Martensite needles
Austenite
60 m
x
x
x
x
x
x
potential
C atom sites
Fe atom
sites
Adapted from Fig. 10.22, Callister & Rethwisch 8e.
• Isothermal Transf. Diagram
• g to martensite (M) transformation..
-- is rapid! (diffusionless)
-- % transf. depends only on T to which rapidly cooled
10
10
3
10
5
time (s)
10
-1
400
600
800
T(ºC)
Austenite (stable)
200
P
B
TE
0%
100%
50%
A
A
M + A
M + A
M + A
0%
50%
90%

## Slide 13: Martensite Formation
 (FCC)  (BCC) + Fe3C
slow cooling
tempering
quench
M (BCT)
Martensite (M) – single phase
– has body centered tetragonal (BCT) crystal structure
Diffusionless transformation BCT if C0 > 0.15 wt% C
  BCT  few slip planes  hard, brittle

## Slide 15: Phase Transformations of Alloys
Effect of adding other elements
  Change transition temp.
Cr, Ni, Mo, Si, Mn
retard    + Fe3C
reaction (and formation of pearlite, bainite)
Adapted from Fig. 10.23, Callister & Rethwisch 8e.

## Slide 17: Summary of Possible Transformations
Adapted from Fig. 10.36, Callister & Rethwisch 8e.
Austenite (g)
Pearlite
(a + Fe3C layers + a
proeutectoid phase)
slow
cool
Bainite
(a + elong. Fe3C particles)
moderate
cool
Martensite
(BCT phase
diffusionless
transformation)
rapid
quench
Tempered
Martensite
(a + very fine
Fe3C particles)
reheat
Strength
Ductility
Martensite
T Martensite
bainite
fine pearlite
coarse pearlite
spheroidite
General Trends

## Slide 18: Phase transitions Aluminum-copper alloys
Harry Bhadeshia
Haixue Yan
photograph courtesy of Sunita Hansraj from her Antarctica expedition

## Slide 19
Ref: Phase transformations in metals and alloys, third edition, DAVID A. PORTER, KENNETH E. EASTERLING, and MOHAMED Y. SHERIF

## Slide 21
Ref: Phase transformations in metals and alloys, third edition, DAVID A. PORTER, KENNETH E. EASTERLING, and MOHAMED Y. SHERIF

## Slide 22
Ref: Phase transformations in metals and alloys, third edition, DAVID A. PORTER, KENNETH E. EASTERLING, and MOHAMED Y. SHERIF

## Slide 23
Ref: Phase transformations in metals and alloys, third edition, DAVID A. PORTER, KENNETH E. EASTERLING, and MOHAMED Y. SHERIF

## Slide 24: Example: Al-Cu alloy
• Internal wing structure on Boeing 767
• Aluminum is strengthened with precipitates formed by alloying.
Adapted from Fig. 11.26, Callister 7e.
(Fig. 11.26 is courtesy of G.H. Narayanan and A.G. Miller, Boeing Commercial Airplane Company.)
1.5mm
Adapted from chapter-opening photograph, Chapter 11, Callister 5e. (courtesy of G.H. Narayanan and A.G. Miller, Boeing Commercial Airplane Company.)
Precipitation hardening
Ref: Materials Science and Engineering,
I version, William D. Callister, David G. Rethwisch

## Slide 25: Effect on phases and mechanical properties
’ GP (Gunnier-Preston ) zones”’CuAl2()
GP: fine scale enrichment with Cu atoms
” : fine scale precipitate, large locale lattice distortion, coherent, elastic, very effective barriers to dislocation movement, peak hardness
’ : as ” disappear ’ form. Partially coherent, hardness reduces
 : CuAl2 precipitate, equilibrium phase.
Ref: Materials Science and Engineering,
I version, William D. Callister, David G. Rethwisch

## Slide 26: Optimum heat treatment
A series of experiments should be done by tempering the quenched samples at different temperatures and different duration. Then the yield strength or hardness of the samples should be measured and plotted as in the sketch.
Ref: Materials Science and Engineering,
I version, William D. Callister, David G. Rethwisch

## Slide 27: PBL
Describe, with the aid of sketches, the heat treatments, phase diagram, microstructure and mechanical properties for the precipitation hardening of Al-Cu alloys. Your answer should identify the important requirements to achieve good precipitation hardening.