## Slide 1
Part IB
Materials Science and Metallurgy
Course A: Metals & Alloys
Professor Harry Bhadeshia
Lecture 10: Iron Alloys

## Slide 2
body-centred cubic (ferrite)
cubic close-packed (austenite)

## Slide 3
DISPLACIVE
RECONSTRUCTIVE

## Slide 6
Carbon in octahedral interstices in austenite

## Slide 7
Carbon in irregular octahedral interstices in ferrite

## Slide 8
Chatterjee & Bhadeshia, 2006

## Slide 11
Yamasaki & Bhadeshia, 2004

## Slide 13
20 µm

## Slide 17
20 µm

## Slide 22
1200
1000
800
600
400
200
0
Pearlite
Martensite
Bainite
kilocycles to Crack Initiation
Yates, Jerath

## Slide 23
Yates, Jerath

## Slide 25
UPPER BAINITE
(High Temperature)
LOWER BAINITE
(Low Temperature)
Carbon supersaturated plate
Carbon diffusion into
austenite
Carbon diffusion into
austenite and carbide
precipitation in ferrite
Carbide precipitation
from austenite

## Slide 26
200 Å
g
g
a
a
a
Mateo, 2002

## Slide 27
Cambridge University / Science Musuem, London