USER’S MANUAL FOR 3-D MONTE CARLO GRAIN GROWTH PROGRAM.

I. How to run the program

OPTION 1: Run the as received compiled code

The isothermal Monte Carlo simulation program can be run by double clicking on the file isograin.exe. It is not necessary for the user to have any compiler to run this code. For those users who want to make changes in the source code and use the program, the following are some tips about compiling and running the program in Digital Visual Fortran.

OPTION 2: Recompile and run the code in Digital Visual Fortran

Open a New workspace from the File menu and click the Fortran Standard Graphics or QuickWin application option. Now choose the QuickWin application option and click OK to create a new workspace. From the menu bar select ProjectAdd to projectFiles option and then add isograin.f, topology.f, averages.f and dialog.rc to the source files. Similarly add resource.h to the header files category. Make sure that all the above mentioned files and the files, comblock.f and resource.fd are in the same directory. Now compile and link them to create isograin.exe. The executable is now ready to run.

OPTION 3: Recompile and run the code in any other FORTRAN compiler

For running with any other compiler (without the visual interface) make the isograin.f subroutine as main and remove the run subroutine. Also remove the if-endif statement enveloping the default input in the isograin.f subroutine and remove the ‘USE’ statements in all the subroutines. The input parameters can also be read in from a file input.dat. For doing this go to line #185 and replace the statement

data compdat/100,100,100,48,100,26,923,40.e-6,10,0.8,13.0,2.0e19,0.0/

with

open(23,file = ”input.dat”)

read(23,*) (compdat(i), i=1,13)

II. Background

Grain structure is an important microstructural feature of a material. It contributes to strength, ductility, toughness, and corrosion resistance. Due to its importance, grain growth has been a topic of much research. In recent years work has also been done to model grain growth using computer simulation with a Monte Carlo algorithm [1-6]. A Microsoft Windows based computer program for the calculation of grain growth in three dimensions has been developed using Monte Carlo technique.  Calculations of certain topological features are performed along selected planes. These features are the frequency distribution of number of sides of each grain (topological class distribution), the angles between adjacent sides, change of perimeter (total length of grain boundary) with time and the grain size distribution. The topological calculations are done in two dimensions. The simulation is done using Digital Visual Fortran. A graphical user interface (GUI) has been built using Quick Win environment. The basic concepts of calculation, some special features of the calculation, a flow chart (appendix 1), a guide to using the GUI, input data, abbreviated output files, and results for an example are provided in the following sections.

III. Basic Concepts

III.1. Monte Carlo Simulation of Grain Growth

The application of the MC technique to simulate grain growth have been described in detail in the literature [1-6]. Only the salient features of this technique are described here. Each of the grid points is assigned a random orientation number between 1 and Q, where Q is the total number of grain orientations. A grain boundary segment is defined to lie between two sites of unlike orientation. In other word, two adjacent grid points having the same orientation number are considered to be a part of the same grain; otherwise they belong to different grains. The grain boundary energy is specified by defining an interaction between nearest neighbor lattice sites. The local interaction energy, E, is calculated by the Hamiltonian:

E=-Jj=1n(dSiSj−1)			             (1)

where J is a positive constant which sets the scale of the grain boundary energy,  is the Kronecker’s delta function, Si is the orientation at a randomly selected site i, and Sj are the orientations of its nearest neighbors, and n is the total number of the nearest neighbor sites. The sum is taken over all nearest neighbors. Each pair of nearest neighbor contributes J to the system energy when they are of unlike orientation and zero otherwise. The Kronecker’s delta function in equation (1) is defined as:

dSiSj=1			(Si = Sj)		(2)

dSiSj=0			(Si  Sj)		(3)

The kinetics of grain boundary migration are simulated by selecting a site randomly and changing its orientation to one of the nearest neighbor orientations based on energy change due to the attempted orientation change. The probability of orientation change is defined as:

p = 1			       E  0			 (4)

p = exp(-E/kBT)               E > 0			 (5)

where E is the change of energy due to the change of orientation, kB is the Boltzman constant, and T is the temperature. Successful transitions at the grain boundaries to orientations of nearest neighbor grains thus corresponds to boundary migration.

In three dimensional simulation, the total number of the nearest first, second and third neighbors is 26 as shown in Fig. 1. The energy difference due to attempted orientation switching is calculated by:

ΔE=Ji=126δSiS0−δSiSn					  (6)

where S0 is the original orientation number, Si are the orientation numbers of its nearest neighbors, Sn is a new orientation number.  According to equation (6), the energy change (E) due to attempted orientation switching will be determined by the energy scale (J) and the energy levels i=126δSiS0−δSiSn. It should be noted that the grain boundary energy is treated as isotropic in equations (1) and (6). The consideration of the anisotropic grain boundary energy is also included in the present model, which is described in detail in section III.3.

III.2 Isothermal Grain Growth Kinetics from MC Simulation

Through the MC simulation, an empirical relation1 between the simulated grain size and the MC simulation time can be obtained as:

L=K1×λ×tMCSn1                                                 (7)

where L is the simulated grain size measured by mean grain intercepts,  is the discrete grid point spacing in MC technique, tMCS is the MC simulation time or MC simulation iteration steps, K1 and n1 are the model constants, which are obtained by regression analysis of the data generated from MC simulation. It should be noted that equation (7) represents the intrinsic grain growth kinetics of the MC model dependent only on the grid system of the MC model and independent of material properties and temperature-time history.  The MC simulation time (tMCS) in equation (7) is a dimensionless quantity.

Recently first efforts have been made to extend the three dimensional Monte Carlo simulation model for grain growth to materials experiencing steep temperature gradients. Two different materials namely commercially pure titanium [7,8] and a 2.25Cr-1Mo [9] steel have been investigated for various welding conditions. The calculated grain structures in both the cases and the grain size and topological class distributions for the commercially pure titanium weld agreed very well with corresponding experimental data.

III.3 Anisotropic Nature of Grain Boundary

The grain boundary anisotropy may have a significant influence on grain growth.  In order to incorporate anisotropy into the Monte Carlo (MC) model, two principal methods have been used that consider anisotropic grain boundary energy or anisotropic grain boundary mobility. The grain boundary energy is highly dependent on the misorientation of two grains abutting the grain boundary and the orientation of a boundary plane [10]. Depending on the systems investigated, the effects of grain boundary misorientation or the orientation of the boundary plane can be introduced separately or in combination. For high purity materials, the grain boundary mobility can be considered to be orientation independent. In other words, the grain boundary mobility is isotropic. Only the anisotropic grain boundary energy needs to be considered. In this case, the grain boundary energy is considered to be a function of grain misorientation. By doing so, the simulation results will be valid for pure materials and doped materials when anisotropic mobility effects are negligible.

In the MC procedure considering anisotropic grain boundary, the energy of a grain boundary as a function of the grain misorientation across the boundary [10] is expressed as:

E=-V(q)j=1n(dSiSj−1)		            	     (8)

where V() is a yet unspecified local anisotropy potential, which is defined below in equations (10) and (11),  is the Kronecker’s delta function, Si is the orientation at a randomly selected site i, and Sj are the orientations of its nearest neighbors. The sum is taken over n ( = 26 ) nearest neighbor sites.

The orientation dependence of boundary energies can be divided into two categories. One is the dependence on the misorientation of two grains forming the boundary and the other, on the orientation of boundary plane. It is assumed that the grain boundary energy is independent of relative boundary orientation and is strictly a function of relative grain misorientation, . In other word, the grain boundary is assumed to be purely tilt character which means that two adjacent grains can be made to coincide by rotating an axis parallel to the grain boundary. The symbol of  is expressed as [10]:

q=2p(Si−Sj)Q 				                 (9)

where Q is the total number of orientations. The Read-Shockey form of interaction potential V() is used to describe the grain boundary energy as following [10]:

V(θ)=Jθ'θ1−lnθ'θ                         for ’<*     		     (10)

V(q)=J 				       for ’*		   	     (11)

where ' =  for 0 and '  2- for 2, * is that value of misorientation parameter, , above which grain boundaries are considered high angle. Some typical values for * are 12.2 for tin, 25 for lead, 26.6 and 29.8 for the (110) and (100) tilt boundaries in silicon iron, respectively. [11]

#### X

#### Z

#### Y

Fig. 1: The 26 neighbors in the three nearest shells in a cubic grid.

### IV. Code Execution

### A Windows based graphical user interface (GUI) was built using the Quick Win environment provided in Digital Visual Fortran. After the program is executed the following screen comes up:

Press the Start button to continue. The cancel button will stop the execution of the program but will not exit the window. The user can run the program once again or exit the window from the file menu.

The various computational and physical parameters required to run the calculation can be supplied using this dialog box. The default array is set at 100x100x100. This is the maximum array size and the user has to be careful not to exceed it. The Default button will restore the default values for each of the parameters. A large volume of data are generated from each run. These data are classified into several data files. The names of these files can be selected by the user. This task is accomplished by pressing the “Next>>” button.

### This dialog box contains the names and paths of the output files. The default main directory is c:\MC. The subdirectories size and topol contain the grain size and topological information respectively. The files contained in the directory size are Mgsize.dat and Gsdist.dat. The contents of the files are described below.

##### Mgsize.dat

This file contains the mean grain size as a function of time. For calculating average grain size, six x, y, and z planes selected by the user are considered. The grain size is calculated by a lineal intercept method. In each plane, grain intercepts along alternate grid lines that are orthogonal to each other are considered. Then the average value of all intercepts is taken as the grain diameter.  The first few lines of the file are reproduced below:

Average grain size (micro meter) after iteration #     1=   5.511739

Average grain size (micro meter) after iteration #     2=   6.007339

Average grain size (micro meter) after iteration #     3=   6.673794

Average grain size (micro meter) after iteration #     4=   7.564608

Average grain size (micro meter) after iteration #     5=   8.574632

Average grain size (micro meter) after iteration #     6=   9.816949

Average grain size (micro meter) after iteration #     7=   11.00261

Average grain size (micro meter) after iteration #     8=   12.09904

Average grain size (micro meter) after iteration #     9=   13.10013

Average grain size (micro meter) after iteration #    10=   14.03883

.      .

.      .

.      .

Gsdist.dat

In any given plane there is a distribution of grain size with grains ranging from very small to very large with an average grain size R. A measure of the grain size distribution (R/R} averaged for the six planes selected by the user is provided in the file Gsdist.dat. The values of R/R range from 0.1 to 3.4. In order to calculate frequency, these values are divided into 34 segments with an interval of 0.1. The frequency is counted as the number of data points within each interval. The user can normalize the frequency with respect to the total number of data points. The first few lines of the file are reproduced below:

Iteration #         200

Range of (D/Davg)   Frequency

0.1000000       4.833333

0.2000000       3.166667

0.3000000       4.166667

0.4000000       3.333333

0.5000000       3.833333

0.6000000       4.833333

0.7000000       6.833333

0.8000000       5.333333

0.9000000       7.000000

1.000000       4.666667

.                .

.                .

The files contained in the directory topol are: a) Gridindex.dat, b) Perimeter.dat, c) Nosides.dat, and d) Anglesides.dat.

Gridindex.dat

In any plane each grain is identified by a unique serial number starting from one. The serial numbers of all the grains in a single selected plane (the last of the six planes selected by the user with plane Z = 66 being the default) is provided in this file. The first few lines of this file containing the orientation number, IQ, and the grain serial number, INDX, for each grid location are reproduced below:

VARIABLES="I","J","IQ","INDX"

Zone I=         100,J=         100,F=POINT

1           1          48           1

1           2          48           1

1           3          48           1

1           4           7           2

1           5           7           2

1           6           7           2

1           7           7           2

1           8           7           2

1           9          24           3

1          10          24           3

1          11          24           3

1          12          24           3

1          13          24           3

1          14          24           3

1          15          20           4

.           .           .           .

.           .           .           .

Perimeter.dat

The total length of grain boundary in each of the six selected planes decreases with time. Since square grids are considered for each selected plane, the perimeter of each grain can be calculated by summing up the maximum orthogonal grain intercepts for each grain and multiplying the sum by two. A measure of the sum of the perimeters of all grains (total length of grain boundary) per unit area as a function of time is provided in file Perimeter.dat. The first few lines are the reproduced below:

Perimeter/unit area after iteration #     10(in mm/sq.mm) =   6.051753

Perimeter/unit area after iteration #     20(in mm/sq.mm) =   5.168887

Perimeter/unit area after iteration #     30(in mm/sq.mm) =   4.567677

Perimeter/unit area after iteration #     40(in mm/sq.mm) =   4.120595

Perimeter/unit area after iteration #     50(in mm/sq.mm) =   3.849428

Perimeter/unit area after iteration #     60(in mm/sq.mm) =   3.623798

Perimeter/unit area after iteration #     70(in mm/sq.mm) =   3.435621

.             .                .           .           .

.             .                .           .           .

Nosides.dat

In any given plane there is a distribution of number of sides of a grain with grains having three to more than ten sides. A measure of the distribution of number of sides of a grain averaged for the six planes selected by the user is provided in this file. The number of edges of a grain are equivalent to the number of neighboring grains of a grain To get a measure of the length of each side and also the total length of the grain boundary, a variation of cluster enumeration program [3] can be used. The program, first, locates and counts all the grids of a given orientation (q value), which are contiguous and indexes them. It then specifically counts those grids that envelop a grain. Then the program calculates the length of each side by calculating the distance between the grids at grain corners while moving along the peripheral grids of a grain. The number of sides was found to range from 3 to 13 for the example cited in this document. In order to calculate the frequency of grains with a particular number of sides, these values are divided into 10 segments with an interval of 1. The frequency is counted as the number of grains within each interval. The user can normalize the frequency with respect to the total number of grains. The first few lines of the file are reproduced below:

*****************************

Iteration #         100

****************************

Number of sides  Frequency

3.000000       1.666667

4.000000       3.333333

5.000000       10.50000

6.000000       42.50000

7.000000       38.00000

8.000000       11.83333

9.000000       5.833333

10.00000       2.500000

11.00000       2.666667

12.00000       1.666667

- 2.500000

Aveneig.dat:

In this file the average number of sides of every grain in the plane are listed. Since grains grow in relation to their neighbors, it is important to study the topology of the neighboring grains.

Grain Index		No.of sides	Average no.of sides of neighbors

1           6      4.750000

2           4      6.000000

3           7      5.000000

4           6      6.600000

5           4      7.333333

6           7      4.500000

7           3      6.000000

8           4      5.000000

.           .       .

.           .       .

Avgedg.dat:

In this file the grain size for each and every grain in the domain is listed as a function of the number of sides of that grain.

Grain Index		No.of sides		Grain Size

1        6.000000       800.0000

2        4.000000       420.0000

3        7.000000       360.0000

4        6.000000       580.0000

5        4.000000       220.0000

6        7.000000       300.0000

7        3.000000       140.0000

8        4.000000       400.0000

.         .                .

.         .                .

The orientation data for all grid points in the six user selected planes, are written in six data files whose names can be selected by the user. This task is accomplished by pressing the “Next>>” button.

### The orientation data obtained after the completion of Monte Carlo calculations for X = c1, Y = c1, Z = c1, X = c2, Y = c2, and Z = c2 planes, where c1 and c2 are the plane numbers, are given in the files indicated in the above dialog box. The default values of c1 and c2 are 33 and 66 respectively. For example the file containing orientation data for the plane X =33 are given in “OrienX33.dat” and stored in the subdirectory orien. The data in these files are used for topological calculations. These files can also be used to obtain a map of the grain structure using an appropriate visualization program. The first few lines of OrienX33.dat which contains grain orientation data for the X = 33 plane are reproduced below:

VARIABLES="X","Y","Z","IQ"

Zone I=         100,J=         100,K=           1,F=POINT

33           1           1          48

33           1           2          48

33           1           3          48

33           1           4           7

33           1           5           7

33           1           6           7

33           1           7           7

33           1           8           7

33           1           9          24

33           1          10          24

.           .          .           .

.           .          .           .

.           .          .           .

### The rest of the files look similar to OrienX33.dat. Now press the Run Code button to start the execution of the program. To show the progress of the program, the number of cumulative successful reorientation attempts is show for each time step. Similarly for the topological part number of grains in each selected plane is shown for every time step. The first few lines of the output obtained on the screen is given below:

THE 3D MONTE CARLO

SIMULATION

PROGRAM

Developed by S. Sista, Z. Yang and T. DebRoy

The Pennsylvania State University

The time now is:          17:          56:          22

Mcstep   Cumulative successful

reorientations

1           0

2      862015

3     1589617

4     2252401

5     2887860

6     3519034

7     4154960

8     4800537

9     5456314

10    6120276

.         .

.         .

Mcstep  Total number

of grains

1        5642

1        5550

1        5628

1        6950

1        7095

1        6991

2        4000

2        3839

2        3959

2        5482

2        5476

2        5478

3        2946

.         .

.         .

Monte Caro Simulation Finished.

The time now is:          20:          32:          41

The Time taken is :           2:           36:           19

Finally a review dialog appears to ask the user about performing another calculation. Pressing the Yes button will take the user back to the initial dialog box and pressing the No button will end the calculations. To end the program completely the user has to go to the file menu and then choose the exit option.

V. Results:

The program was run for a 100x100x100 grid for 100 iterations, with a maximum of 48 orientations at a constant temperature of 923 K and a grid spacing of 40 m. The physical and computational parameters are given in table 1. Since the MC simulation results can vary from run to run, the grain growth and topological results presented in this paper are averaged over 5 runs to examine this variation. The run to run variations of results are indicated by error bars in the figures. Topological attributes and the average grain size were determined in the following six planes: X = 1.32 mm, Y = 1.32 mm, Z = 1.32 mm, X = 2.64 mm, Y = 2.64 mm and Z = 2.64 mm in the 4 mm4 mm4 mm domain. Lineal intercept method [14] was used in the calculation of average grain size. In each plane, alternate grid lines served as test lines. Thus, there were a total of one hundred test lines with fifty lines being orthogonal to the other fifty lines. The number of grains intercepted by each line was counted. For example, in the Z = 2.64 mm plane, the number of grains intercepted by all the test lines was 1990 for 125 minutes (7500 s) and 995 for 625 minutes (37500 s), respectively. The total length of the hundred lines (400 mm) was then divided by the total number of intercepted grains to get the average grain size for any specific plane.

The simulated grain structure for the 100x100x100 grid as a function of time is shown in Fig. 2. This figure was obtained using Tecplot visualization software from the orientation files for X =0 mm, Y = 0 mm and Z = 0 mm planes. The calculated results for average grain size and grain perimeter per unit area as a function of time and the experimental data are shown in Fig. 3. As expected the mean grain size increases with time and the average perimeter decreases with time as shown in Fig. 3.. The computed grain size distribution data in Fig. 4 also matched very well with experimental results for zone-refined iron [13]. The grain topology is examined in two dimensions in the present study. The distribution of number of sides or the topological class distribution is shown in Fig. 5. It can be observed from the figure that most of the grains in the domain are five sided which agrees very well with the experiments. Fig.6 shows linear relationships when the grain size is plotted as a function of average number of sides per grain. The horizontal dashed lines in the figure indicate the calculated average grain size for the two times taken from Fig. 3. It can be seen that the average grain size corresponds to grains with six sides. In order to examine the effect of the geometry of the neighboring grains on grain topology a plot of the average number of sides of neighboring grains, nn, and the inverse of the number of sides of grains, 1/nr is presented in Fig. 7. Linear relationships were obtained between nn  and 1/nr.

Fig. 2. Evolution of three dimensional simulated grain structure with a 100x100x100 grid system as a function of time.

Fig. 3. Calculated and experimentally determined [12] average grain size and the computed grain perimeter as a function of time.

Fig. 4. The grain size distribution as an average of five runs from the present simulation compared with Hu’s data [12] for zone refined iron.

Fig. 6. The distribution of number of sides of a grain from the present simulation compared with Hu’s data  [12] for zone refined iron.

Fig. 6. The average grain size of a grain as a function of number of sides of a grain, n, for 125 minutes (7500 s) and 625 minutes (37500 s) at 923 K for the plane Z = 2.64 mm. Also represented are the average grain sizes (Ravg) for 125 minutes (7500 s) and 625 minutes (37500 s) taken from Fig. 3.

Fig. 7. Average number of sides of neighboring grains, nn, as a function of the inverse of number of sides, 1/nr, for 125  and 625 minutes (7500 s and 37500 s) at 923 K for the Z = 2.64 mm plane.

| Table 1: Computational and material parameters used in the calculations. The numbers in the parentheses indicate the references from which the values have been taken. |  |
| --- | --- |
| Parameter | Value |
| Grid spacing,  (m) | 40 |
| Total number of grain orientations, q | 48 |
| Initial average grain size, Lo (m) | 40 (13) |
| Number of iteration steps | 200 |
| Temperature (K) | 923 (12) |
| Simulation constant, K1 | 1.01 |
| Simulation constant, n1 | 0.42 |
| Experimental grain growth exponent, n | 2.0 (13) |
| Activation energy (kJ/mol) | 250 (12) |
| Pre-exponential factor, K (m2/s) | 528 (13) |

VI. References

- J. Gao and R. G. Thompson: Acta Metall., 1996, vol. 44, pp. 4565-4570.

- M. P. Anderson, D. J. Srolovitz, G. S. Grest, and P. S. Sahni: Acta Metall., 1984, vol. 32,  pp. 783-791.

- D. J. Srolovitz, M. P. Anderson, P. S. Sahni, and G. S. Grest: Acta Metall., 1984, vol. 32, pp.793-802.

- Y. Saito and M. Enomoto: ISIJ International, 1992, vol. 32, pp. 267-274.

- B. Radhakrishnan and T. Zacharia: Metall. Mater. Trans. A, 1995, vol. 26A, pp. 167-180.

- G. S. Grest, D. J. Srolovitz, and M. P. Anderson: Acta Metall., 1985, vol. 33, No.3, pp. 509 -20.

- Z. Yang, J. W. Elmer, J. Wong and T. DebRoy: Weld. J. Res. Suppl, 2000, vol. 79, No. 4, pp. 97s-112s.

- Z. Yang, S. Sista, J. W. Elmer and T. DebRoy: accepted for publication in Acta. Mater., August 2000.

- S. Sista, Z. Yang and T. DebRoy: Metall. Mater. Trans. B, 31B, 529 (2000).

- G. S. Grest, D. J. Srolovitz, and M. P. Anderson: Acta Metall., 1985, vol. 33, No.3, pp. 509 -20.

- W. T. Read: Dislocations in Crystals, McGraw-Hill, New York, 1953.

- H. Hu, Can. Metal. Q., 13, 275 (1974).

- R. A. Vandermeer and H. Hu, Acta Metal. Mater., 42, 3071 (1994).

- Annual Book of ASTM Standards., 1, Sect. 3, ASTM, West Conshohoken, PA (1996).

APPENDIX 1

E1-E0<=0?

Calculated for all

time steps?

Done with all the grid points?

Accept the reorientation and change the orientation initial site to ior2.

Change the initial Orientation (ior0) to attempted orientation (ior2).

Input Data ( imax, jmax, kmax,iqmax,imcmax,T,,,)

Assign a random orientation number to each site (1~Iqmax)

Randomly select a point (ix,iy,iz) in the lattice and note its orientation as ior0

Find the neighbors of the selected site

Calculate local interaction energy before reorientation (E0)

Select a new random orientation (ior2) for the site from the neighbors

and then calculate the local interaction energy (E1)after reorientation.

Output results for visualization (Tecplot format)

No

Yes

Count the Mcsteps (i)

Yes

No

No

Yes

One MC Step

End

APPENDIX 2

Frequently Asked Questions (FAQ's)

1) How reliable is the random number I use?

The subroutine random_number(argument) returns one pseudo random number or an array of pseudo random numbers from the uniform distribution over the range 0  x  1. The argument must be a real number. It may have a single value or an one dimensional array. It is set to contain pseudo random numbers from the uniform distribution over the range 0  x  1.

2) I have a workstation with UNIX operating system. How do I modify the source code to run it in the UNIX operating system?

For running in the UNIX operating system (without the visual interface) make the grainiso subroutine as main and remove the run subroutine. Also remove the if-endif statement enveloping the default input in the grainiso subroutine and remove the ‘USE’ statements in all the subroutines. The input parameters can also be read in from a file input.dat. For doing this goto line #185

And replace the statement

data compdat1/100.,100.,100.,48.,100.,26.,923.,40.e-6,10.,0.8,13.,2.0e-19,0.0/

with

open(23,file=”input.dat”)

read(23,*) (compdat(i), i=1,13)

While compiling the files grainiso.f, averages.f and topology.f in a UNIX operating system, the files dialog.rc and resource.h are not required.

3) I am using a HP 9000 machine and the FORTRAN 77 compiler does not seem to recognize the random number subroutine. What should I do?

The random number generator which can be used in the HP 9000 work station using a FORTRAN 77 compiler is an intrinsic function nrand48 (). It has been taken from the 'C' language library. The function nrand48 () returns positive long integers uniformly distributed over the interval, 0  random number < 231. By using different seeds, the nrand48 function allows separate modules of a large program to generate independent sequences of pseudo-random numbers. In other words, the sequence of numbers that one module generates does not depend upon how many times the function is called by other modules. This problem doesn't seem to exist when using the FORTRAN 90 compiler on a HP workstation. For more information, please consult the manual for your FORTRAN compiler.