## Slide 1: Aluminium-copper alloys
Harry Bhadeshia
Haixue Yan
Phase transitions

## Slide 2: encounter with Michael Cook
about 3 cm in length
Darwin College

## Slide 3
reproduced with permission of Cllr Peter Dace, Northshaw & Cuffley Parish Council
https://northawcuffleypc.org.uk/w-l-robinson-vc/
Royal Flying Corps personnel examining the debris from the

## Slide 4: corrugated for engineered rigidity

## Slide 5: Duralumin
an aluminium-(10Cu wt%...+Mg, Mn) alloy invented and patented by Alfred Wilm, a Berlin Chemist, in 1906
First produced in Düren (Prussian territory), hence, Duralumin (pronuounced douralumin)
Heat it to say 500°C, quench, leave. It hardens at room temperature over a period of days

## Slide 6
solution

## Slide 7: Microscopy & microanalysis

## Slide 8: Microanalysis
Aluminium contains copper, magnesium and silver additions

## Slide 9
solution
Age hardening: fine precipitates
dissolve solute
controlled heat treatment
precipitate in fine form

## Slide 10
suitability for age hardening
A
B

## Slide 11
red phases metastable
meaning?
why does metastable form at all?
why does solubility change?

## Slide 14
Bob Waugh

## Slide 16
Equilibrium compositions using the common tangent construction.
Metastable precipitate has a greater free energy, than stable one.
Increased solubility of Cu in Al.

## Slide 19: Crystals of liquid? bizarre!

## Slide 20
Crystals: long-range order, anisotropic.
Liquids: no long-range order, isotropic.
Liquid crystals are anisotropic liquids due to molecular shape.

## Slide 22: Example 27: cholesterol (first liquid crystal)
Solid cholesterol heated above 145 °C, forms cloudy liquid.
On reaching 170 °C, it clarifies.
This effect is reverisible.
Explain.

## Slide 23: Solution 27
Liquid crystal has aligned molecules. Different regions have different orientation. Therefore, scatter light, cloudy.
At higher temperature, disorder, true liquid, so no domains to scatter light.